## Slide 1: Elevated Temperature Mechanical Properties of L-PBF Niobium Alloy: C103
Justin L. Milner and Eric Brizes
NASA Glenn Research Center, Cleveland OH
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Orlando, FL March 3-7, 2024
National Aeronautics and Space Administration

## Slide 2: Introduction
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
NASA Refractory Alloy Projects:
  STMD-GCD – Refractory Alloy Additive Manufacturing Build Optimization (RAAMBO)
  Hypersonic Technology (HTP) Project.
    Advance material characterization and prototypic testing allowing for critical data needed to demonstrate TRL advancement and for component flight qualification
    Enable national supply chain for refractory alloy feedstock essential for production of historical to custom alloys for R&D to component fabrication.
    Develop materials and processing for high performance in extreme environments enabling technologies for Moon to Mars missions.
  Alignment with NASA Projects:
  Fission Surface Power (FSP) – High temp. core and power conversion materials
  Nuclear Electric Propulsion (NEP) - Core, power conversion and thruster materials
  Nuclear Thermal Propulsion (NTP) - Extreme environment materials
  In-Situ Resource Utilization (ISRU) - High temp. materials for lunar systems
  Hypersonic Technology’s (HTP) - Ox-compatible refractory metals
  Lander ascent/descent and RCS nozzles
  This work:
  Focuses on AM process development for L-PBF C103
  Determine elevated temperature mechanical properties for L-PBF C103
  Microstructural evaluation of tested materials.

## Slide 3: C103 Powder Feedstock
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Chemical composition of C103 powder
C103 powder feedstock physical properties
Powder morphology of gas atomized Nb alloy, C103

## Slide 4: L-PBF of C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Schematic of build layout
As-built C103 tension blanks
EOS M100
Energy density of 10.1 J/mm3

## Slide 5: Density of L-PBF C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
As-Built
HIP
AM built C103 physical properties

## Slide 6: Chemical Composition
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Chemical composition of C103 powder, AM C103, and wrought C103

## Slide 7: High Temperature High Vacuum Tension Testing Rig
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Testing Procedure
Load Sample
3x argon purge
High vacuum (diffusion pump)
Heat up at 5x10-6 Torr or better at a rate of 17 °C/min
Soak at temperature for 20 minutes
Constant crosshead speed of 6.35x10-3 mm/s

## Slide 8: Tension of Wrought and AM C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Wrought C103
AM C103

## Slide 9: Tension of Wrought and AM C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Wrought C103
AM C103
DNF = Did not fail

## Slide 10: Tension of Wrought and AM C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Wrought and additively manufactured C103 mechanical properties

## Slide 11: High Temperature High Vacuum Creep Testing Rig
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
Testing Procedure
Load Sample
3x argon purge
High vacuum (Turbo pump)
Cold sample measurement
Heat up at 5x10-6 Torr or better at a rate of 17 °C/min
Soak at temperature for 20 minutes
Hot sample measurement
Apply load
LVR and optical extensometer to track strain

## Slide 12: Creep of Wrought and AM C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
1300°C at 50 MPa
LMP of 1% Creep Strain
[1] R.H. Titran and W.D. Klopp, 1980
[1]

## Slide 13: Microstructure of AM C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
As-Built
HIP

## Slide 14: EBSD of Wrought C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
As-Worked
Recrystallized

## Slide 15: EBSD of AM C103
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
As-Built
HIP

## Slide 16: Conclusion
TMS 2024 153RD ANNUAL MEETING & EXHIBITION
C103 spherical powder feedstock was able to be printed to high theoretical density by L-PBF. C103 samples were printed and tested at elevated temperature in tension and creep in the as-built and HIP conditions. Wrought C103 was also tested for comparison.
AM and HIPed C103 displayed large grain growth and oxide coarsening after processing. HIP parameters are not considered optimized for this material.
In general, AM C103 shows similar strength to wrought C103 when comparing AM as-built to wrought as-worked and AM HIPed to wrought recrystallized. Main takeaway is that AM C103 does exhibit slightly increased strength at elevated temperatures beyond 1000°C. And AM C103 exhibits decreased ductility over wrought C103. This may be attributed to 5-8x higher oxygen content in the AM C103.
Creep testing of AM and HIPed C103 displays increased creep performance over wrought recrystallized C103. This may be attributed to the larger grain size and 8x higher oxygen content of the AM C103.