## Slide 1: Influence of Stoichiometry on Zirconium Oxycarbides (ZrCxOy) Exposed to Hot Flowing Hydrogen
Martin Volz1, J. K. P. Williams1,A. Croell2, J. Reynolds1, B. Taylor1, J. Rosales1, E. Kardoulaki3 and K. J. McClellan3
1NASA Marshall Space Flight Center
2University of Alabama in Huntsville
3Los Alamos National Laboratory

## Slide 2: Motivation
ZrC is anipated to be a primary NTP nuclear reactor material, eticither as a constituent in a solid solution binary carbide (UZrC) or tricarbide (ex. (UZrNb)C), or as a coating.
Hyper- or hypo- stoichiometries of carbon in (UZr)C carbides can decrease the melting point and operational temperature range.
Oxygen can be unintentionally incorporated into a mixed carbide either as a component in the starting powder, or through oxidization during powder processing or sintering of the solid.
Quantitative data is lacking on the effects that oxygen incorporation and carbon concentration have on mass loss rates and material structure when ZrCxOy is exposed to hot flowing hydrogen.
Lyon, Los Alamos Scientific Laboratory
Report LA-5398-MS (1973)
How critical is the oxygen and carbon concentration in carbide NTP reactor fuel?

## Slide 3: Sample Preparation
Sample ZrC23-1 was prepared with stoichiometry from powders as-received from vendors.
  ZrC0.95O0.03
Sample ZrC23-2 was prepared by first heating ZrC powder in air to increase oxygen concentration.
  ZrC0.83O0.14
Sample powders consolidated by Spark Plasma Sintering resulting in 40 mm diameter by 6 mm tall billets.
4 rectangular test specimens were cut from each billet after polishing for testing in hot hydrogen at different temperatures.
Samples characterized by oxygen and carbon elemental analysis, XRD, density measurements, and SEM/EDS at each stage of processing.
Cut-out pattern
Sample ZrC23-1B

## Slide 4: X-Ray Diffraction Results
None of the samples show evidence of any secondary phases (e.g., ZrO2)
Oxygen can sit at a carbon site in the ZrCx lattice forming the zirconium oxycarbide (ZrCxOy)
Oxygen and Carbon concentration cannot be determined directly from XRD but were determined by inert gas fusion (oxygen by LECO ON836, carbon by Horiba EMIA-PRO)
Oxygen concentration can affect the sample density and lattice spacing (not discernable on graph)

## Slide 5
Hot Hydrogen Compatibility Test System
Compact Fuel Element Environmental Test (CFEET)
  Testing in flowing Hydrogen at 6 SLPM
  Testing to date at 2300 K and 2600 K
  Multi-spectral pyrometry (FAR Associates) for temperature measurements
  Pyrometers viewing from top and side
  Side View
  Top View

## Slide 6: Density Changes from Hot Hydrogen Exposure
Oxygen rich samples had a lower density after SPS but increased in density upon hot hydrogen exposure.
Lower oxygen concentration samples decreased in density upon hot hydrogen exposure.
Samples exposed to higher temperatures had a lower density.

## Slide 7: ZrCxOy Mass Loss Rates (MLR’s)
Factors Affecting MLR
Sample density
Diffusion rates of Zr, C, and O
Activity (vaporization) of ZrCxOy in hydrogen
Gas pressure
Chemical reactions
2H2 + C → CH4
H2 + 2C → C2H
2H2 + 2C → C2H4
2H2 + O2 → 2H2O

## Slide 8: Acknowledgements
The current work was completed at NASA - Marshall Space Flight Center and supported by NASA’s Space Technology Mission Directorate (STMD) through the Space Nuclear Propulsion (SNP) project
The University of Alabama in Huntsville was involved in the research and was supported by NASA under cooperative agreement NNM11AA01A