## Slide 1: Arc Jet Test Article Instrumentation AM-TPS Workshop 3.0
Jose Santos, Josh Monk
NASA Ames Research Center
1-May-2024

## Slide 2: Outline
TPS Instrumentation Overview
Sensor types
  Technical considerations
  Availability
  Facility considerations
Examples
  Stagnation, shear, and panel test articles
Application
  Thermal Response Models
Summary

## Slide 3: TPS Instrumentation
For spaceflight missions involving atmospheric entry, the environment experienced by a spacecraft cannot be fully replicated on the ground
Taking measurements in the flight environment is the “gold standard” for:
  Validating predictive modeling tools
  Reducing risk on future EDL missions
Instrumenting arc jet models with TPS sensors provides critical data needed for:
  Development and validation of material response models
    Ground-to-flight traceability analysis
  Evaluation of sensor performance
  Demonstrating “Do No Harm” to the TPS
MEDLI instrument suite
Orion EFT-1 heat shield

## Slide 4: Sensor types

## Slide 5: Thermocouples (TCs)
Measurement quantity:
  Temperature difference between hot and reference junctions by measuring voltage arising from the Seebeck effect
Sensor considerations:
  Measurement range is dependent on TC type (see ASTM E230 standard)
  Type K, R, S, and C are most commonly used
Availability:
  Good to Fair for COTS item from various vendors
  Produced in-house at NASA ARC with laser weld at the hot junction (upon request)
Facility considerations:
  Passive sensor  no power excitation
  Susceptible to noise or extraneous currents if embedded in conductive TPS material
  Typical installation into TPS material via TC plug
Metal 1 (+)
Metal 2 (-)
Thot
Tref
Measure voltage here
TC bead weld (“hot junction”)
Type K: -200 to 1,260 C
Type R or S: 0 to 1,480 C
Type C: 0 to 2,315 C

## Slide 6: Thermocouple (TC) Plugs
TC plug can be installed into a counterbore with adhesive or press-fit
Lead wires fed through the thickness to route to data acquisition system
Can also be installed via threaded design (higher density materials) or through-hole (instead of counterbore) and substrate
Adhesive or press-fit
Counterbore hole
Thermocouple plug fabrication at NASA Ames
X-ray image
See ASTM E377 for low-conductivity TPS materials

## Slide 7: Pressure Transducers
Measurement quantity:
  Absolute or differential pressure
Sensor considerations:
  Piezoresistive strain gage-based measurement is common
  Specialized units (e.g., variable reluctance) for very low pressure applications (hundreds of Pascal)
  Often requires temperature compensation
Availability:
  Good to Fair for COTS items from various vendors
  Very few choices for spaceflight ready transducers
    Difficulty with cold temperatures (< -120 C)
Facility considerations:
  Form factor and size
  Calibration
  Integration within arc jet test article
MEDLI / MEDLI2 Hypersonic transducer
Kulite brand pressure transducer
Orion EFT-1 pressure transducer
Artemis 1 shoulder pressure transducer

## Slide 8: Heat Flux Sensors and Radiometers
Sensor Considerations:
  Radiometers typically incorporate a window to block out convective heating
  If installed at the surface, deposition of TPS ablation/pyrolysis products on the window will alter the heat flux measurement
Availability
  Fair, only a few select reputable vendors
Facility Considerations:
  Pre-run checkouts and DAS setup
  Calibration
Measurement quantity:
  Total heat flux sensor: combined convective and radiative heating
  Radiometer: radiative component of heating
  Direct measurement of heat flux
    Voltage output calibrated with radiant heat source
EFT-1 Heat shield Radiometer
MEDLI2 Backshell Radiometer
MEDLI2 Backshell Total Heat Flux Sensor

## Slide 9: Recession Sensors
Measurement quantity:
  Direct or inferred recession of TPS material
Sensor considerations:
  Discrete vs continuous recession measurement
  Calibration process is not well established
  Accuracy better than  +/- 0.1 cm not attainable with current higher TRL options
Availability:
  No ready-made COTS solutions
  NASA custom designs flown/will fly on specific flight missions (MEDLI, Artemis II)
  Low TRL concepts from SBIRs or other R&D efforts
Facility considerations:
  Power excitation and DAS setup
  Pre-run checkouts
  May need to rely on arc jet run video or other diagnostics to compare with sensor response
TPS
Photo diodes
UV from shock layer
Ablation direction
Optical Recession Sensor (ORS)
Hollow aErothermal Ablation and Temperature (HEAT) sensor

## Slide 10: Examples

## Slide 11: Stagnation Test Articles
Wide range of test article designs have been tested in the arc jet facilities
  Successful measurements made with TC plugs, active pressure ports, heat flux sensors, and recession sensors
TPS model
Water cooled housing
Electronics subassembly
Simple Design
Complex Design
Flat face geometry
Single TC plug installed in the center
No power excitation
“Iso-Q” curved OML geometry
Electronics packaging
Power excitation
TC Plug
TPS model
Insulator
Mounting plate

## Slide 12: Wedge Test Articles
Wedge test articles need a water-cooled holder assembly
  Leading edge and side frame pieces
  “Plug-and-play” adapter available for additional interior volume to house sensors
“Wedge” shear test configuration in IHF. Test article with TC plug shown.
Exploded view of CAD design of wedge pressure port test article
CAD image of assembled wedge pressure port test article
“Plug-and-play” adapter
Test article OML surface exposed to flow  4.2” x 4.5”
Total TPS test coupon thickness limited to  1.3”
TC Plug

## Slide 13: Panel Test Articles
TC Plug
Pressure Port Plug
Heat flux Sensor in TPS plug
Various pressure port holes
Substructure material
Heat flux Sensor
TPS material
12”x12” PTF test article
8”x10” TFD test article
Larger test articles can accommodate multiple sensors, but max. test conditions are lower than IHF or AHF
TC Plug

## Slide 14: Application

## Slide 15: Validation of Material Models with Ground Test Data
Material response analysis is leveraged for thermal protection material sizing for flight projects
It is critical to evaluate the predictive capabilities for the TPS models using ground testing as flight conditions cannot be fully replicated and modeling must be used for TPS design
Confidence of the material response models are derived from comparisons with thermocouple data at relevant flight conditions
  In-depth temperature predictions
  Recession predictions
Uncertainties and margin policies are also informed by these comparisons and sometimes updates to material models are recommended to reduce risk

## Slide 16: Examples of Material Response Analysis Approaches
CFD informed in-depth comparison
TC Data used as direct boundary condition
Multiple TCs for in-depth comparisons
CFD informed conditions allow for comparison of cool down predictions
Shallow TCs are another opportunity to validate model recession predictions when TC burn out occurs
Limitations:
TPS coating effects may add uncertainties in comparisons
Complex facility conditions may lead to aerothermal environment uncertainties
Decouples impact of coatings in model comparison
TC driver approach allows for easy side-side comparison for material response models
More TCs allow for TC1, TC2 etc. driver simulations
Limitations:
Simulations only run as long as TC data is available
TC burn out leads to short simulations and in-depth comparisons may not be relevant (plan conditions and run times accordingly)
TC1
TC2
Low Condition PTF Instrumented Test
Measured data
Material Response Predictions
IHF High Condition Instrumented Test
Pyrometer
0.10”
0.20”
0.45”
0.70”

## Slide 17: Summary
There are many important considerations for the design of an instrumented arc jet test article
  Traceability to TPS material or flight instrumentation test objectives
  Test configuration (stagnation, wedge, panel)
  Number and type of sensors
  Facility interfaces
Arc jet facility has experience with several different sensor types
  Examples: thermocouples, pressure transducers, heat flux sensors, recession sensors
Instrumented TPS ground test provides critical data used to validate TPS material response models for future flight missions

## Slide 18: Back Up

## Slide 19: Additional Resources
Contact information:
  Jose Santos: jose.a.b.santos@nasa.gov
  Josh Monk: joshua.d.monk@nasa.gov
ASTM standards:
  ASTM E230: https://www.astm.org/e0230_e0230m-17.html
  ASTM E377: https://www.astm.org/e0377-08r20.html
  ASTM E21.08 subcommittee: E21.08 Jurisdiction Page (astm.org)
    Many standards on heat flux measurement relevant to ground tests