## Slide 1: The two-cavity method for characterizing acoustical materials—an interlaboratory study
Martha C. Brown NASA Langley Research Center, Hampton, VA | Anthony Ciletti Wichita State University, Wichita, KS | Janith Godakawela and Bhisham Sharma Michigan Technological University, Houghton, MI

## Slide 2: Evolution of Aircraft Engine Noise
The evolution of the relative dominance of various acoustic sources
as the engine bypass ratio (BPR) has increased.
1960s
1:1 BPR Engine
1990s
6-8:1 BPR Engine
2000s
12:1 BPR Engine
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Source: Epstein, Alan, “The Lessons of P&W’s Geared Turbofan Engine and the Implications for the Future,” Keynote Address, International Symposium on Air Breathing Engines (ISABE), Phoenix, AZ, October 2015.

## Slide 3: Conventional Liner Locations
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Single-Layer Liner
Core Flow
Bypass Flow
Acoustic Liners
Aircraft Engine Nacelle
Perforate
Facesheet
Honeycomb
Core
Backplate

## Slide 4: Current Broadband Acoustical Materials
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Organic Foams
Hybrid Foams
Inorganic Foams
Inorganic Fibers
Hybrid Fibers
Organic Fibers
Conventional bulk absorbers
Underlying porous architecture is incidental to the fabrication process.
Fabrication methods limit:
    Microstructural optimization
    Material optimization
    Functionality optimization
Various types of commonly used porous acoustical materials.

## Slide 5: Characterizing Porous Materials
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Porous media needs to be uniform for analysis purposes.
When the intrinsic parameters are known, then the surface impedance can be predicted for any thickness.
Intrinsic Parameters
= Characteristic Impedance
G = Propagation Constant
Characterization Methods
Two-Thickness Method
  TWO samples
Two-Cavity Method
  ONE sample + 2 cavity depths

## Slide 6: Triply Periodic Minimal Surfaces
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Potential multifunctionality
Load bearing + Thermal management + Energy absorption + Acoustic absorption?
TPMS heat exchangers*
Inlet View
Outlet View
*Reference: nTopology.com

## Slide 7: Triply Periodic Minimal Surfaces
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Design and build tunable bulk materials for aerospace applications.
  Focus on Triply Periodic Minimal Structures (TPMS).
  Tunable to desired frequency range of interest.
  Focus on acoustic benefits where traditional designs are not feasible. (i.e., multifunctionality, installation on other locations in an engine)
Benefits
  Additive manufacturing facilitates the ability to control the TPMS characteristics.
  TPMS structures can be modeled.

## Slide 8: Sample Selection and Fabrication
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Diamond
All samples were fabricated using stereolithography.
Samples were printed with porosities of 40% and 60%.
Sample thickness: 2 in, 60% porosity
1.5 in square sample
2.0 in active square sample
Iso View
Top View

## Slide 9: Overview of Interlaboratory Study
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Same Design
Stereolithography (SLA)
+ Accura60 Resin
Stereolithography (SLA)
+ Formlabs Clear V4 Resin
Two-Cavity Method
Normal Impedance Tube
Normal Impedance Tube
Assume: Uniform Sample
Measured Results
Measured Results
Characterization Method

## Slide 10: Test Rigs
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Capabilities:
Sound pressure levels (SPL): 120 and 140 dB
Sound Source: tonal (stepped-sine, swept-sine, multi-tone) and broadband
Frequency range of 500 to 3000 Hz
Eduction Method: Two-Microphone Method
Capabilities:
Sound pressure levels (SPL): 100 dB
Sound Source: tonal (stepped-sine, swept-sine, multi-tone) and broadband
Frequency range of 500 to 3000 Hz
Eduction Method: Two-Microphone Method
Mecanum Normal Impedance Tube
1.5 in square samples
LTF Normal Impedance Tube
2.0 in square samples
Rotating Plug
Sample Installation
Source
Measurement

## Slide 11: Overview of Two-Cavity Method
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Cavity of depth L
Cavity of depth L’
Characteristic Impedance
Propagation Constant

## Slide 12: Overview of Two-Cavity Method
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Cavity of depth L
Cavity of depth L’
Characteristic Impedance
Propagation Constant
Cavity Depths Explored: 0.5, 1.0, 2.0 in

## Slide 13: Overview of Two-Cavity Method
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Cavity of depth L
Cavity of depth L’
Characteristic Impedance
Propagation Constant
SAME analysis code used on separate datasets.

## Slide 14: Demonstration of Sample Linearity
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
NASA Printed, Sample thickness = 2 in.
40% porosity
60% porosity

## Slide 15: Comparison of Measured Results
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Sample thickness = 2 in.
40% porosity
60% porosity

## Slide 16: Comparison of Measured Results
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Sample thickness = 2 in, 0.0 in cavity
40% porosity
60% porosity
Differences indicate further investigation is required.

## Slide 17: Comparison of Measured Results
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Sample thickness = 2 in, 0.0 in cavity
40% porosity
60% porosity

## Slide 18: Comparison of Measured Results
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Sample thickness = 2 in, 0.0 in cavity
40% porosity
60% porosity
Frequency range of interest can be targeted by tuning porosity.
Differences indicate further investigation is required.

## Slide 19: Explore intrinsic properties of samples
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Sample thickness = 2 in, 60% porosity, Cavity depth combinations: 1 in and 2 in

## Slide 20: Explore intrinsic properties of samples
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Sample thickness = 2 in, 60% porosity, Cavity depth combinations: 1 in and 2 in
Notes: Remove the real and imaginary component.
Keep the units.

## Slide 21: Comparison of Measured vs Prediction
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Sample thickness = 2 in., 60% porosity, Cavity depth combinations: 1 in. and 2 in.
Acquire impedance data for cavity depth.
Acquire impedance data for cavity depth.
Use Two-Cavity Method to calculate and .
Use and to predict the surface impedance of a 2 in sample with no cavity depth, .
Compare to with no cavity depth.

## Slide 22: Overview of Interlaboratory Study
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Sample thickness = 2 in., 60% porosity, 0.0 in cavity
Notes: NASA=> issue with the application of the two-cavity method (need further investigation)

## Slide 23: Concluding Remarks
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
The interlaboratory study demonstrated the importance of collaboration for the purpose of improving modeling techniques.
Differences in measured results between the Liner Technology Facility and MADLab demonstrate the need to better understand as-designed and as-built samples.
More analysis is needed to properly use the Two-Cavity Method on TPMS structures.

## Slide 24: Future Work
Introduction | TPMS Structure | Experimental Method | Results | Conclusion | Future Work
Reduce additive manufacturing error by using the same parent material and source printer.
Conduct a deep-dive into the phase unwrapping process.
Explore optimal two-cavity combinations for the Two-Cavity Method.
Integrate the Two-Thickness Method into the investigation to better refine the Two-Cavity Method process.
Testing: Consistent SPLs and type of sound source.

## Slide 25: Acknowledgments
Advanced Air Transport Technology Project (AATT)
of the NASA Advanced Air Vehicles Program for funding this work

## Slide 26
Notes: NASA Presentation Sign-Off Page