## Slide 1
Thermal Radiator Electrodynamic Dust Shield
PI: Dr. Krystal Acosta
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, FL 32899
Dr. Joseph Toth
Dr. Tracy Gibson
Dr. Charles Buhler
Jerry Wang
James Phillips
Dr. Aaron Olson
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024

## Slide 2: Electrostatic forces dominate at smaller particle sizes
Notes: Apollo 17 Harrison Jack Schmitt coated with dust
Apollo 17 Eugene Cernan in lunar module after an EVA

## Slide 3: wo
There are two main types of radiators: reject heat or absorb heat
3
Light Reflected
Heat Emitted
Heat Absorbed and emitted
Limited Light Reflected

## Slide 4: Dust hinders the radiator’s ability to reject heat
4
4
Dust
Light Reflected
Heat Emitted
Heat Absorbed
Limited Light Reflected
“As little as 12 percent dust coverage can degrade the α [solar absorptance] by as much as 50 percent.”1
Radiator
EDS
Coating
  1Gaier et al. NASA Technical Memorandum, “The Effect of Simulated Lunar Dust on Absorptivity, Emissivity, and Operating Temperature on AZ-93 and Ag/FEP Thermal Control Surfaces, 2008
Limited Light Reflected
Heat Absorbed and emitted
Limited Light Reflected
Some Heat Absorbed
Dust

## Slide 5: The EDS is a technology that uses high alternating electric fields to remove particles
Electrodynamic Dust Shield (EDS):
Insulating layer
Electrodes
Substrate
Adhesive
Ground/ Other Phase
Out-of-Plane (3D) EDS:
In-Plane (2D) EDS:
Insulating layer
Electrodes
Substrate
Robust
Higher voltage
Thicker
Fragile
Lower voltage
Thinner
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024

## Slide 6: Coating properties need to align with EDS requirements
Key coating properties for thermal radiator coatings:
Key coating properties for EDS:
Solar Absorptance, α
Emittance, ε
Adhesion
Thin – particles close to the traces
Electrically Insulative
High Dielectric Strength
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024
UV resistance

## Slide 7
MISSE-11 AZ-93
MISSE-15 Thermalbright
Some coatings have been exposed in space on the ISS

## Slide 8
Stack up:
Manufactured EDSs using a thermal evaporator and laser etching
Kapton MT tape if necessary*
Copper Electrodes*
Kapton MT+ (thermally conductive)*
Adhesive: 3M 8926*
Aluminum Plate (Radiator)
Thermal control coating
*not necessary for regular thermal radiator

## Slide 9: Testing
Several tests were conducted:
Solar Absorptance/ Emissivity
Dust Removal in air/ vacuum
Surface and Volume Resistivity
Dielectric Breakdown
Thermal Vacuum

## Slide 10
Solar White
AZ-93
A276
Thermal Bright
White Kapton
The coatings have standard dry thicknesses which can affect thermal optical properties
Barium Sulfate
Chart: Solar Absorptance (%)
| AZ-93 0.15 mm | AZ-93 0.22 mm | Barium Sulfate 0.03 mm | Barium Sulfate 0.08 mm | Solar White 0.05 mm | Solar White 0.12 mm | A276 | White Kapton Gloss | White Kapton Matte | Thermalbright
EDS | 17 | 16.7 | 18.7 | 14.3 | 21.3 | 16.7 | 20.3 | 29.9 | 36.3 | 24.5
Without EDS | 17.5 | 16 | 16.5 | 14 | 18.5 | 15 | 19.5 | 29.7 | 34.7 | 25.7
Chart: Emittance (%)
| AZ-93 0.15 mm | AZ-93 0.22 mm | Barium Sulfate 0.03 mm | Barium Sulfate 0.08 mm | Solar White 0.05 mm | Solar White 0.12 mm | A276 | White Kapton Gloss | White Kapton Matte | Thermalbright
EDS | 92.7 | 91.3 | 89 | 89.7 | 88 | 87.3 | 88.7 | 87.7 | 87.3 | 87.7
Without EDS | 92.5 | 91.5 | 58.5 | 76 | 81.5 | 84.5 | 88 | 87.5 | 88 | 86.5
EDS
Without EDS

## Slide 11
Solar White
A276
Thermalbright
Barium Sulfate
Dust removal testing was conducted in air and vacuum
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024
Two methods of determining dust removal: image intensity and mass lost
 | Vacuum | 
Coating | Image Intensity Clearing (max %) | Mass loss clearing (max %)
AZ-93 0.15 mm | 44% | 75%
AZ-93 0.22 mm | 9.0% | 45%
Barium Sulfate 0.03 mm | 98% | 96%
Barium Sulfate 0.08 mm | 98% | 103%
Solar White 0.05 mm | 79% | 85%
Solar White 0.12 mm | 53% | 61%
A276 | 91% | 90%
White Kapton Gloss | 67% | 65%
White Kapton Matte | 49% | 31%
Thermalbright | 42% | 45%
Vacuum Testing:
Pressure: 1x10-4- 10-6 Torr
Voltage: ± 1-2 kV
Frequency: 10 Hz
Operation:
AC square wave
DC for 1 minute (polarization)
AC square wave

## Slide 12
Solar absorptance returned to near normal values when the EDS worked
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024
Chart: Solar Absorptance recovery after dust removal in vacuum
| AZ-93 0.15 mm | AZ-93 0.22 mm | Barium Sulfate 0.03 mm | Barium Sulfate 0.08 mm | Solar White 0.05 mm | Solar White 0.12 mm | A276 | White Kapton Gloss | White Kapton Matte | Thermalbright
Clean | 17 | 16.7 | 18.7 | 14.3 | 21.3 | 16.7 | 20.3 | 29.9 | 36.3 | 24.5
With Dust | 77.3 | 72.7 | 70.7 | 69.3 | 45.3 | 48 | 63
After Dust | 34 | 55 | 23 | 20.5 | 29 | 37 | 26.5 | 47 | 49 | 47.7
Emissivity values did not change with or without dust
  Coatings and dust both have high emissivity values
Clean
With Dust
After Dust

## Slide 13
The voltage required to breakdown increased with the addition of the EDS
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024
Chart: Breakdown Voltage at >50% RH
| AZ-93 0.22 mm | Barium Sulfate 0.08 mm | Solar White 0.12 mm | A276 | White Kapton Gloss | White Kapton Matte | Thermalbright
Aluminum | 0.68 | 1.3 | 0.57 | 3 | 6.2 | 5.9 | 5.9
EDS | 5.1 | 5.9 | 5.3 | 8.13 | 6.7 | 6.8 | 6.5
Coated aluminum
Coated EDS on aluminum
All coatings insulative in vacuum (AZ-93 and solar white statically dissipative at 50% RH)

## Slide 14
Thermal vacuum tests indicate a different adhesive is necessary for EDS functionality
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024
Thermal profile:
EDS did not function after reaching steady state
Chart: PID Control Thermocouple
Further testing necessary to determine the thermal impact the EDS has on the radiator performance (effective emittance)

## Slide 15: Future work will refine the EDS radiator stack up and conduct thermal testing
Conclusion:
Tested various coatings on EDSs bonded to radiators
  Measured dust clearing, thermal optical properties with and without dust
    Solar absorptance measurements returned to within 10% of starting value after dust removal on the best coating EDS combinations
Future testing
Effective emittance of the EDS with a thermal control coating
New adhesives to mitigate delamination at higher temperatures
Testing a functional thermal radiator with a coolant loop with the EDS
Scaling up the EDS to a full-size radiator used in space
Radiator
EDS
Coating
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024
EDS mats made by Hedgefog Research Inc.

## Slide 16: Thank you! Questions?

## Slide 17: Backup
Absorptance: amount of light absorbed by sample, accounts for reflectance and transmittance
Absorbance: log of the incident light vs transmitted light, does not tell anything about reflectance or absorption, measures attenuation
Absorption: act of being absorbed

## Slide 18
Clean baseline
After re-duster
To determine amount of dust removal:
Clearing efficiency,
Pristine
Added dust
Removed dust
- baseline intensity
- image with dust
- image after clearing
Looking into taking solar absorptance and emittance measurements before, during, and after dusting process
The amount of dust cleared is determined through image intensity and mass loss
2024 Joint Conference on Electrostatics, Ottawa, Canada June 9-13, 2024
Mass Lost equation: