## Slide 1: Monodisperse Single-Material Granular Tribocharging Modeling and Experimental Validation
James Phillips1
Jessica Schwend1, David Lund1, Robert Frady1, Krystal Acosta1, Joseph Toth1, Aaron Olson1, Jerry Wang1, Charles Buhler1, Sid Clements2, Tarek Elgohary3, Adrienne Dove3
1NASA Kennedy Space Center
2Appalachian State University
3University of Central Florida
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 2: Background
Understanding grain tribocharging under vacuum is of interest for space applications
Developing models to determine how lunar dust will charge and be deposited
Experiments are required to bound results from these simulations
Asymmetry in granular systems lead to charge transfer:
  Size asymmetry is known well [Lacks, 2011; Bilici, 2014]:
    smaller particles tend to charge negatively
    larger particles tend to charge positively
  Contact asymmetry will be further examined here:
    more dynamic particles tend to charge positively
    more static particles tend to charge negatively
    previously discussed at 2013 ESA Annual Meeting [Buhler, 2013]
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 3: Applications to Modeling/Simulations
LIGGGHTS1 granular mechanics discrete element method (DEM) modeling software implements many mechanical interactions between particles, but neglects inter-particle electrostatics [Kloss, 2012]
We have incorporated basic electrostatics interactions (conduction, basic tribocharging, and screened Coulomb force) into LIGGGHTS in previous works [Phillips, 2021; Wang, 2022]
Tribocharging relation implemented from literature [Mukherjee, 2016; Laurentie, 2013]:
  Driven by difference in work function, , of contacting particles
  Charge transfer occurs when overlap area, , is maximized
  Magnitude limited by a cutoff distance for charge transfer,
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
1 Large-scale Atomic/Molecular Massively Parallel Simulator (LAMMPS) Improved for General Granular and Granular Heat Transfer Simulations (LIGGGHTS®) is a registered trademark; DCS Computing GmbH is the official producer of the LIGGGHTS® software; LIGGGHTS®-PUBLIC is provided under the GNU General Public License v2.0
This behavior is incomplete and results in particles with identical work functions remaining neutral (unlike reality)
Contact detection will be implemented and linked to charging

## Slide 4: Experimental Overview
Tray filled with insulating spherical glass beads is slowly inclined
Beads rub against one another as they pour out of tray opening
Beads leaving tray fall and are captured inside Faraday cup
Net charge of all beads within cup is monitored with electrometer
Polarity of beads remaining in tray is confirmed with field meter
After system equilibrates, mass of beads in cup is measured
Overall charge-to-mass ratio is computed
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
Faraday
Cup
Motor
Vacuum Chamber

## Slide 5: Experimental Challenges
Beads bouncing out of Faraday cup
  Anti-static foam was added to bottom of cup to stop beads from escaping
Isolating beads from wall interactions
  Double-sided tape was used to coat inside of tray with identical beads
Assuring neutrality of all beads before beginning the experiment
  First Experiments: beads added to tray in layers and neutralized with ionizer fan after each layer
  Later Experiments: beads neutralized with ionizer fan directly as they were poured into tray
  Field meter was used to verify neutrality of particle bed before starting experiment
Larger particles tend to avalanche all at once compared to smaller particles
  Attempted to run experiments multiple times until clean capture, but data for larger particles is sparse
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 6: Experimental Setup: Tray Design
Several profiles were examined to limit avalanching and minimize wall interactions
Worked well to vary flow rate of particles, but significant particle-wall charging was still measured
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 7: Experimental Setup: Wall Isolation
Double-sided tape was used to adhere layer of particles to wall of tray
Ensures particles only interact with other particles and not tray walls
Open front profile prone to avalanching of large particles, but necessary
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
Faraday
Cup
Motor
Double Sided Tape
Vacuum Chamber

## Slide 8: Experimental Results: Mass Flow Rate
Beads were poured out of tray into container on calibrated load cell in atmospheric conditions
Majority of mass flow occurs in 2 minutes, but experiment will be limited to first 100 seconds when mass flow rate is roughly linear
  Avoids wall effects toward end of flow
  Mass flow rate averages around
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
Notes: 6-21-23\MassFlowRate

## Slide 9: Experimental Results: Larger Particles
3mm diameter glass beads under high vacuum:
  Larger particles have fewer interactions and do not charge to the same degree as smaller ones
  Avalanching occurred in green run, so not as many contacts were made and charge was low
Net charge in cup is positive in all cases
  Ranges between 1 and 4 nC for similar mass
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
 | Charge (nC) | Mass (g) | Q/m (pC/g)
Trial 1: | +3.7 | 280 | 13
Trial 2: | +2.6 | 295 | 8.8
Trial 3: | +1.4 | 295 | 4.7
Mean: | +2.6 | 290 | 9.0
Notes: 7-17-23: larger particles, avalanching, differently shaped tray opening

## Slide 10: Experimental Results: Refined Opening
1mm beads were poured out of aluminum and plastic trays in high vacuum conditions
Net charge in cup is positive in all cases
  Ranges between 23 and 35 nC for similar mass
Aluminum vs plastic tray did not differ significantly
Determined square opening is best config
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
 | Charge (nC) | Mass (g) | Q/m (pC/g)
Trial 1: | +25.8 | 320* | 81*
Trial 2: | +23.9 | 320* | 75*
Trial 3: | +34.5 | 320* | 108*
Mean: | +28.1 | 320* | 88*
*assumed mass
Notes: 6-16-23\electrometer\square_edge: switched to smaller beads and square front opening

## Slide 11: Experimental Results: Before Tape
1mm beads were poured out of plastic tray in atmospheric conditions
Net charge in cup is positive in all cases
  Ranges between 7 to 11 nC for similar mass
  Interactions with walls dampen charging
Tape added to plastic tray to minimize wall effects
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
 | Charge (nC) | Mass (g) | Q/m (pC/g)
Trial 1: | +8.7 | 320 | 27
Trial 2: | +8.6 | 320 | 27
Trial 3: | +10.5 | 320 | 33
Trial 4: | +7.6 | 320 | 24
Trial 5: | +7.0 | 320 | 22
Mean: | +8.5 | 320 | 27
Notes: 6-21-23\Plastic_Air

## Slide 12: Experimental Results: After Tape
1mm beads were poured out of taped tray in atmospheric conditions
Net charge in cup is positive in all cases
  Ranges between 16 to 26 nC for similar mass
More interactions because tape limits sliding
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
 | Charge (nC) | Mass (g) | Q/m (pC/g)
Trial 1: | +25.4 | 320 | 79
Trial 2: | +19.7 | 320 | 61
Trial 3: | +16.0 | 320 | 50
Trial 4: | +20.3 | 320 | 63
Mean: | +20.4 | 320 | 64
Notes: 6-22-23\tape

## Slide 13: Experimental Results
1mm diameter glass beads under high vacuum:
  Higher net charge for 1mm vs 3mm particles
Net charge in cup is positive in all cases
  Ranges between 19 and 36 nC for similar mass
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
 | Charge (nC) | Mass (g) | Q/m (pC/g)
Trial 1: | +35.2 | 194 | 181
Trial 2: | +25.4 | 199 | 128
Trial 3: | +19.4 | 186 | 104
Trial 4: | +24.7 | 202 | 122
Trial 5: | +27.1 | 209 | 130
Mean: | +26.4 | 198 | 133

## Slide 14: Simulation Setup
Reconciling experimental results with models by implementing contact detection and counting
Cohesion between grains and tray walls was set to large value
  Enforces grains to be tangent to tray surface
  Does not limit sliding/rolling motions
Coefficients of friction between grains and tray walls were set to large value
  Prohibits grains from sliding/rolling along tray surface
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
Cohesion Energy Density () |  | 
 | Wall | Grain
Wall | 0 | 
Grain |  | 0
 | Wall | Grain
Wall | 0 | 
Grain |  | 0
Coefficient of Rolling Friction |  | 
 | Wall | Grain
Wall | 0 | 1
Grain | 1 | 0
Coefficient of Sliding Friction |  | 
 | Wall | Grain
Wall | 0 | 1
Grain | 1 | 0

## Slide 15: Simulation Example
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 16: Simulation Challenges
Mesh objects in LIGGGHTS must all have identical physics applied
  Tray behaves as if covered with double-sided tape [intended]
  Faraday cup also covered in double-sided tape [unfortunate]
Contacts inside Faraday cup are still counted and cause artificial inflation of numbers
Mitigations:
  Trajectories of particles in XZ plane are plotted as function of time
  Intersections with YZ plane indicating free fall of particle recorded
  Time step at which this occurs is used to look up number of contacts per particle
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 17: Simulation Preliminary Results
Bimodal distribution of per-particle contacts seen when comparing beads inside Faraday cup to those remaining behind in tray
Though preliminary, can be related to bipolar nature of charge segregation in monodisperse systems
Average number of contacts for beads on walls of tray was higher than for those collected in cup
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
 | Total Contacts | Total Beads | Average Contacts | Full Width Half Max
Remaining in Tray | 3958740 | 833 | 4752 | ~2000
Inside Faraday Cup | 7441878 | 2687 | 2769 | ~6000

## Slide 18: Summary
All experiments indicated positive charge on beads in Faraday cup and negative charge in tray
Particles that are more dynamic charge positively (i.e. those that slide/roll out of tray)
Particles that are more static charge negatively (i.e. those left behind in tray)
Improvements still needed to align simulations with experimental results
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
-
+
-
-
-
-
-
-
-
+
+
+
+
+
+

## Slide 19: Future Work
Perform additional tests with different materials than only glass beads
Improve contact counting in simulations to align with experimental data
  Better discriminate between static and dynamic particles in simulations
    Track static-dynamic and dynamic-dynamic bead contacts separately
  Place limits on number of interactions per grain to simulate saturation of charge
Decrease sizes of and increase number of particles in simulation to align with experiments
Investigate scenarios other than only pouring grains
  Fluidized beds, vacuuming up/blowing off surface grains, etc.
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 20: References
Bilici, M.A., Toth III, J.R., Sankaran, R.M., Lacks, D.J. 2014. “Particle size effects in particle-particle triboelectric charging studied with an integrated fluidized bed and electrostatic separator system.” Review Scientific Instruments, 85(10):103903.
Buhler, C.R., Clements, J.S., Deckman, H., Dougal, S., Lamberti, W., Moebus, J., Reynolds, R. 2013. “New Observations on the Bipolar Nature of Charge Segregation in Triboelectrically Charged Granular Materials.” Electrostatics Society of America 2013 Annual Meeting.
Kloss, C., Goniva, C., Hager, A., Amberger, S., Pirker, S. 2012. “Models, algorithms and validation for open-source DEM and CFD–DEM.” Progress in Computational Fluid Dynamics, 12(2–3):140–152.
Lacks, D.J., Sankaran, R.M. 2011. “Contact electrification of insulating materials.” Journal of Physics D: Applied Physics, 44(45):453001.
Laurentie, J., Traore, P., Dascalescu, L. 2013. “Discrete Element Modeling of Triboelectric Charging of Insulating Materials in Vibrated Granular Beds.” Journal of Electrostatics, 71(6):951–957.
Mukherjee, R., Gupta, V., Naik, S., Sarkar, S., Sharma, V., Peri, P., Chaudhuri, B. 2016. “Effects of Particle Size on the Triboelectrification Phenomenon in Pharmaceutical Excipients: Experiments and Multi-Scale Modeling.” Asian Journal of Pharmaceutical Sciences, 11(5):603–617.
Phillips III, J.R., Wang, H., Hillegass, A., Esparza, A., Dove, A.R., Elgohary, T.A. 2021. “Implementation of Charged Particle Behavior in Discrete Element Method (DEM) Simulations.” ASCE Earth and Space 2021 Conference.
Wang, H., Phillips III, J.R., Dove, A.R., Elgohary, T.A. 2022. “Investigating Particle-Particle Electrostatic Effects on Charged Lunar Dust Transport via Discrete Element Modeling.” Advances in Space Research, 70(10):3231-3248.
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 21: Backup Slides
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024

## Slide 22: Experimental Results: Wall Interactions
3mm beads were poured out of aluminum tray in atmospheric conditions
Net charge in cup is positive in all cases until beads contacting walls fell into cup as well
  Indicates need for double-sided tape
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
Notes: 6-21-23\Alum_Air

## Slide 23: Experimental Results: Wall Interactions
3mm beads were poured out of plastic tray in atmospheric and high vacuum conditions
Net charge in cup is positive in all cases until beads contacting walls fell into cup as well
  Indicates need for double-sided tape
Electrostatics and Surface Physics Laboratory
NASA Kennedy Space Center, Florida
2024 ESA Annual Meeting
Ottawa, Canada June 10-12, 2024
Notes: 6-22-23\plastic