## Slide 1: L’Ralph Early On-Orbit Thermal Performance and Investigation of the Colder-than-Expected Cryoradiator Daniel Bae, NASA GSFC 545 Owen Warner, NASA GSFC 545 OSTEM Intern Juan Rodriguez-Ruiz, NASA GSFC 545
Presented By
Daniel Bae
Thermal & Fluids Analysis Workshop TFAWS 2024 August 26-30, 2024
NASA Glenn Research Center
Cleveland, OH
TFAWS Passive Thermal Paper Session

## Slide 2
The first space mission to explore a population of small bodies known as the Trojan asteroids, which orbit the Sun “in front of” and “behind” the gas giant Jupiter. The Trojan Asteroids are leftovers from the early days of our solar system, effectively the fossils of planet formation. Lucy launched on October 16th, 2021
Lucy
L’Ralph
GSFC in-house instrument on Lucy with two detectors: The visible wavelength multicolor imager (MVIC) and the infrared Linear Etalon Imaging Spectral Array (LEISA), which is passively cooled to 100K. Image below shows temperature zones
MEB 290 K
TDA 170 K
Cryosystem 100 K
IPP 245 K
LEISA Detector
Telescope Detector Assembly (TDA)
Instrument Pointing Platform (IPP)
Main Electronics Box (MEB)
Notes: Lucy will be the first space mission to study the Trojan asteroids associated with Jupiter. It was also launched last year. The L’Ralph instrument on Lucy employs two detectors: The visible wavelength multicolor imager and the infrared Linear Etalon Imaging Spectral Array, which is passively cooled to 100K. The temperature zones of the L’Ralph instrument are shown in the bottom right figure. The coldest cryosystem zone maintained at 100K, while the Telescope Detector Assembly, labeled as TDA is at 170K, the Instrument Pointing Platform - IPP at 245K and the Main Electronics Box - MEB is at 290K.

## Slide 3: L’Ralph Early (<2 AU) On-Orbit Thermal Performance
Cryosystem was showing significantly cooler temperatures
To better understand the thermal performance, instrument pointing platform (IPP) was set at different angles
At low AU, radiative loading from solar array to the cryoradiator dominates the heat flow (>90% of heat input)
  Cryoradiator has a good view to the backside of the solar array backside

## Slide 4: Why is This Happening?
The main theory:
  Directional emissivity curve might have a significant impact
    Cryoradiator has a sharp viewing angle to the solar array, where significant brightness reduction can happen based on the directional emissivity behavior
In the model, Thermal Desktop assumes Lambertian directional emissivity
Solar array directional emissivity may not be Lambertian causing the difference in temperature
Unfortunately, we could NOT test this on ground; solar array is too big and we could not set up a ground test in such a way that would have captured the radiative coupling between L’Ralph and the solar array
Lambertian means that the brightness of the object will remain constant regardless of the viewing angle
Directional emissivity plots from NASA/TP–2005–212792, Kauder, L., “Spacecraft Thermal Control Coatings References”

## Slide 5: Directional Emissivity Measurement using the IR Camera
Chart: Emission Spectrum of Blackbody at 50 °C
IR Camera
Rotational Stage
Vertical Translational Stage
Horizontal Translational Stage
Literature review: Difficulty finding suitable instruments for measuring directional emissivity at <10 degree angles (angle measured from the sample plane)
Ibos et al, Investigation of the directional emissivity of materials using infrared thermography coupled with a periodic excitation
  Discusses a methodology to use an IR camera to measure directional emissivity
  This work utilizes similar test concept
IR cameras measure between approximately 7.5-13 wavelength range
  This is suitable for the solar array radiative coupling investigation; solar array is at about 50 degC, and the planck’s distribution peaks at about 9
Very simple test setup!

## Slide 6: Testing Methodology
IR Camera’s absolute temperature measurement can be inaccurate due to many unknown/unquantifiable sources of heat input
Use relative measurement (Delta Method) to cancel out a lot of the errors!
Chart: Theoretical Calibration Curve of a Sensor
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12 | 12.5
  In addition to canceling unwanted sources of radiation, the delta method also decreases experimental uncertainty
  This is because we don’t have to rely on an absolute temperature calibration, which is more likely to have uncertainties
  Absolute Temperature
  Delta Method
  This Y intercept can be wrong

## Slide 7: IR Camera Energy Balance
IR Camera is a micro-bolometer… and we only care about the radiative heat from the sample
Take two measurements of the sample at two different temperatures and hold everything else constant
  Keep constant by building a temperature controlled shroud around the setup
  Keep and constant by letting camera warm-up for a long time to thermalize before taking any measurements
  Keep constant by making the shroud uniform black and never taking measurements such that the camera would see itself
IR Camera Body with Electronics
IR Sensors
Lens
Sample
Radiation from sample
Radiation from air/surroundings
Radiation from camera body/lens
self heating from the electronics
Reflected radiation off of sample
How would the camera process this?

## Slide 8: IR Camera Internal Data Processing
To get sensible data out of the IR camera, need to go one step further… take the ratio to get rid of additional unknowns:
If we design an experiment such that the hot and cold temperatures are the same between measurements…
And if we keep the camera settings the same between measurements…
And, finally, if we get rid of the coefficients…
Using the approximation: , we can linearize the equation:
Real change in energy received by the camera
Processing of the Radiation Received by the Camera
Note that we still need the normal emissivity value, which we used an in-house instrument to measure

## Slide 9: Test Setup
-
Optical enclosure and Z307 to provide a uniform reflecting surface
Solar Array Sample (Backside)
IR camera
Thermocouples read the temperature of the air, enclosure, IR camera, and sample
Rotation and Translation Stages

## Slide 10: Test Results: Aluminum
  Theoretical directional emissivity curve of a conductor
  Measured Directional Emissivity Curve using the IR camera method

## Slide 11: Test Results: Z307
  Test results from Z307 are consistent with a very diffuse, high emissivity di-electric material
IR Camera measurement methodology and data processing works!

## Slide 12: Solar Array Sample (Backside)
  Kapton/Scrim
  Foam
  Solar Cell

## Slide 13: Test Results: Foam
Experimental data agrees with literature review; significant drop off due to topology
  Emissivity drops off significantly after 40°
Figure taken from Li et al., 2018, “Tomography-based analysis of apparent directional spectral emissivity
of high-porosity nickel foams”
  Consistent with the directional emissivity hypothesis

## Slide 14: Test Results: Kapton
  Kapton/Scrim also experiences a drop of emissivity at glancing angles

## Slide 15: Test Results: Backside of the Solar Cell
  Emissivity increases at glancing angles
  The solar cell has much lower emissivity than the foam and Kapton, so it’s energy contribution to the cryo-radiator is less
  Data from the solar cell is inconclusive and scattered, unknown environmental factors caused two trials to not agree. Needs further investigation

## Slide 16: Directional Emissivity Impact on L’Ralph Thermal Predicts
Inputted directional emissivity curve into the L’Ralph TD model to see its impact on the thermal model predicts
  Used area weighted averaging of the three backside surfaces to generate effective directional emissivity curve
Unfortunately, directional emissivity only partially explains the cooler temperature that we see on flight
Thankfully, at >5 AU, the radiative coupling between the solar array and the cryoradiator drops off by >10x, so for L’Ralph’s science, the reduced radiative coupling should not cause significant impact
More glancing angle between the solar array and the cryoradiator
-75 deg
0 deg
110 deg
SA
Cryorad

## Slide 17: Conclusion
Successful directional emissivity measurement system (for limited spectral range) was developed with very little cost
Significant emissivity drop off at glancing angles is confirmed… however, this only partially explains the cooler temperature
  Lesson learned: Try and do your best to mimic flight like environment, especially for cryogenic instrument; radiative heat load from the solar array was the only thermal heat source we could not verify via ground testing

## Slide 18: Acknowledgements
Huge thank you to Owen Warner, our OSTEM summer intern, for doing amazing work!
Huge thank you to the L’Ralph team for performing custom on-orbit IPP maneuvers for us, and for providing funds