## Slide 1: Development of computational materials workflows for additively manufactured metallic materials to enable accelerated prediction of fatigue performance
George Weber1, Saikumar Yeratapally2, Peter Spaeth1, Erik Frankforter1,
Joshua Pribe3, Brodan Richter1, Edward Glaessgen1
MS&T 2024 Annual Meeting & Exhibition
Pittsburgh, Pennsylvania
October 8, 2024
1NASA Langley Research Center, Hampton, VA
2Science and Technology Corporation, Hampton, VA
3Analytical Mechanics Associates, Hampton, VA

## Slide 2: Basic Fracture and Fatigue Control for Qualification and Certification (Q&C)
Two classical design approaches
(1) Safe Life
(2) Damage Tolerance

## Slide 3: Basic Fracture and Fatigue Control for Qualification and Certification (Q&C)
Basic philosophy [1] :
Acceptance that damage will occur
Adequate system of inspection so the damage may be detected
Adequate strength maintained in the damaged structure
(2) Damage Tolerance
“The extent of damage for residual strength evaluation at any time within the operational life of the airplane must be consistent with the initial detectability and subsequent growth under repeated loads.”
– FAA 14 CFR 25.571
(1) Safe Life
“The safe life approach only applies to parts which define crack initiation as the limit of the useful life, such as rotating parts.”
- FAA AC 33.70-1
“The safe-life design approach, when properly executed, places statistically predictable failures at an extremely remote probability of occurrence. This approach does, however, assume the structure to be flaw free.” [1]
Three basic elements [1] :
Working Wöhler (“S-N”) Curve
Design Loading Spectra
Cumulative Damage Theory
Two classical design approaches
[1] H. Reddick. Safe-life and damage-tolerant design approaches for helicopter structures (1983)
FAA: Federal Aviation Administration

## Slide 4: Basic Fracture and Fatigue Control for Qualification and Certification (Q&C)
Certified life
Two classical design approaches
Loading Amplitude (S)
Cycles to Initiation (Ni)
106
102
103
104
105
Min.
[1] H. Reddick. Safe-life and damage-tolerant design approaches for helicopter structures (1983)
FAA: Federal Aviation Administration
Example S-Ni Curve
(1) Safe Life
“The safe life approach only applies to parts which define crack initiation as the limit of the useful life, such as rotating parts.”
- FAA AC 33.70-1
“The safe-life design approach, when properly executed, places statistically predictable failures at an extremely remote probability of occurrence. This approach does, however, assume the structure to be flaw free.” [1]
Three basic elements [1] :
Working Wöhler (“S-N”) Curve
Design Loading Spectra
Cumulative Damage Theory
Current approaches that cannot account for microstructure must treat this uncertainty in life conservatively
Scatter is typically attributed to weakest link combinations of microstructural features and flaws

## Slide 5: Basic Crystal Plasticity Workflow
Microstructure
Grain morphology and texture generation
Characterization[1]
Preprocessing and discretization
Output and visualization
Global solver
Constitutive model / solver
Plastic flow rule
Saturating hardening law
Boundary conditions
Solution domain
Constitutive parameters
“Material properties”
[1] Image Credit: Wes Tayon, Bryan Koscielny
Workflow is built for modularity
Workflow is built for iteration
Upscaling
Model analysis
Accuracy analysis
Crystal plasticity is one of the most common mesoscale (µm-mm) frameworks for achieving a mapping between structure and property
Life prediction
Crack initiation and growth

## Slide 6: Crystal Plasticity and Q&C
Entry Points
Limitations
Trust
(1)
(2)
(3)
Why is crystal plasticity not playing a significant role in Q&C?

## Slide 7: Crystal Plasticity and Q&C
Entry Points
Limitations
Trust
(1)
(2)
(3)
Why is crystal plasticity not playing a significant role in Q&C?

## Slide 8: Q&C Entry Points for Crystal Plasticity
Difficult to define entry points to Q&C for mesoscale modeling frameworks
Most Q&C examples from industry are not publicly disclosed
General regulations exist but Q&C packages are domain-specific
Regulatory Entry Points
Some Relevant Documents
FAA 14 Part 25
Airworthiness Standards: Transport Category Airplanes
FAA 14 Part 33
Airworthiness Standards: Aircraft Engines
NASA-STD-5019
Fracture Control Requirements for Spaceflight Hardware
NASA-STD-6040
Additive Manufacturing Requirements for Spaceflight Systems
MMPDS
Metallic Materials Properties Development and Standardization
Material Allowables
Cycles to crack initiation
Stress intensity factor thresholds
Basic mechanical properties
Software
NASGRO®*
Fracture Mechanics and Fatigue Crack Growth Software
AFGROW*
Fracture Mechanics and Fatigue Crack Growth Analysis Software Tool
DARWIN®*
Design Assessment of Reliability with INspection
Technical Entry Points
Fracture Mechanics
Primarily test-driven with empirical modeling
Most mesoscale influence is implicit except flaw sizes
*This is not an endorsement by the National Aeronautics and Space Administration (NASA)

## Slide 9: Crystal Plasticity and Q&C
Entry Points
Limitations
Trust
(1)
(2)
(3)
Why is crystal plasticity not playing a significant role in Q&C?

## Slide 10: Limitations in Crystal Plasticity
#1 Missing Physics
Size invariance, Hall-Petch effect
Dislocation transport, starvation, and conservation laws
Slip bands, extrusions/intrusions, and persistent slip bands
Grain boundary transmission and energetics
#2 Lower Scale Effects
Dislocation core effects and key dislocation mechanisms
Accounting for measured initial dislocation density
Nanoscale voids, precipitates, microcracks, and inclusions
Solid solution hardening, compositional effects
#3 Evolution of Microstructural Input
Grain boundary sliding, coarsening, rotation, migration, and local misorientation
Nanoscale changes such as rafting, phase transformations, deformation twinning, and vacancy generation
#4 Fundamentals
Continuum assumption, separation of scales
Decoupling of elastic and plastic constitutive behavior
Orowan’s equation and Schmid behavior
Infinitesimal deformation and strain measures
#6 Extreme Values
Multi-junctions and field localizations are critical
Confidence in discretization and solver near extremes
Nonlocal length scales
#5 Boundary Conditions
Periodicity, self-consistency
Concurrent or hierarchical coupling with higher spatial scale
Statistical equivalence of representative volume elements
Multi-time scale behavior
#7 Computational Cost
>1,000 grains requires supercomputing
CPU and GPU parallelization add user/developer complexity
Global and constitutive time integration accuracy/stability thresholds
#8 Workflow Efficiency
Software integration
Reproducibility is nontrivial
Constitutive relation development requires competence in tensor analysis
Towards the end goal of crack initiation and microstructurally small crack growth
Fatigue indicator parameter-based approaches or explicit crack modeling are typically dependent on crystal plasticity
However, there is a complex interaction of assumptions and limitations in crystal plasticity

## Slide 11: Limitations in Crystal Plasticity
#1 Missing Physics
Size invariance, Hall-Petch effect
Dislocation transport, starvation, and conservation laws
Slip bands, extrusions/intrusions, and persistent slip bands
Grain boundary transmission and energetics
#2 Lower Scale Effects
Dislocation core effects and key dislocation mechanisms
Accounting for measured initial dislocation density
Nanoscale voids, precipitates, microcracks, and inclusions
Solid solution hardening, compositional effects
#3 Evolution of Microstructural Input
Grain boundary sliding, coarsening, rotation, migration, and local misorientation
Nanoscale changes such as rafting, phase transformations, deformation twinning, and vacancy generation
#4 Fundamentals
Continuum assumption, separation of scales
Decoupling of elastic and plastic constitutive behavior
Orowan’s equation and Schmid behavior
Infinitesimal deformation and strain measures
#6 Extreme Values
Multi-junctions and field localizations are critical
Confidence in discretization and solver near extremes
Nonlocal length scales
#5 Boundary Conditions
Periodicity, self-consistency
Concurrent or hierarchical coupling with higher spatial scale
Statistical equivalence of representative volume elements
Multi-time scale behavior
#7 Computational Cost
>1,000 grains requires supercomputing
CPU and GPU parallelization add user/developer complexity
Global and constitutive time integration accuracy/stability thresholds
#8 Workflow Efficiency
Software integration
Reproducibility is nontrivial
Constitutive relation development requires competence in tensor analysis
Towards the end goal of crack initiation and microstructurally small crack growth
Fatigue indicator parameter-based approaches or explicit crack modeling are typically dependent on crystal plasticity
However, there is a complex interaction of assumptions and limitations in crystal plasticity
#1 Missing Physics
Size invariance, Hall-Petch effect
Dislocation transport, starvation, and conservation laws
Slip bands, extrusions/intrusions, and persistent slip bands
Grain boundary transmission and energetics

## Slide 12: Limitations in Crystal Plasticity
#1 Missing Physics
Size invariance, Hall-Petch effect
Dislocation transport, starvation, and conservation laws
Slip bands, extrusions/intrusions, and persistent slip bands
Grain boundary transmission and energetics
#2 Lower Scale Effects
Dislocation core effects and key dislocation mechanisms
Accounting for measured initial dislocation density
Nanoscale voids, precipitates, microcracks, and inclusions
Solid solution hardening, compositional effects
#3 Evolution of Microstructural Input
Grain boundary sliding, coarsening, rotation, migration, and local misorientation
Nanoscale changes such as rafting, phase transformations, deformation twinning, and vacancy generation
#4 Fundamentals
Continuum assumption, separation of scales
Decoupling of elastic and plastic constitutive behavior
Orowan’s equation and Schmid behavior
Infinitesimal deformation and strain measures
#6 Extreme Values
Multi-junctions and field localizations are critical
Confidence in discretization and solver near extremes
Nonlocal length scales
#5 Boundary Conditions
Periodicity, self-consistency
Concurrent or hierarchical coupling with higher spatial scale
Statistical equivalence of representative volume elements
Multi-time scale behavior
#7 Computational Cost
>1,000 grains requires supercomputing
CPU and GPU parallelization add user/developer complexity
Global and constitutive time integration accuracy/stability thresholds
#8 Workflow Efficiency
Software integration
Reproducibility is nontrivial
Constitutive relation development requires competence in tensor analysis
Towards the end goal of crack initiation and microstructurally small crack growth
Fatigue indicator parameter-based approaches or explicit crack modeling are typically dependent on crystal plasticity
However, there is a complex interaction of assumptions and limitations in crystal plasticity
#5 Boundary Conditions
Periodicity, self-consistency
Concurrent or hierarchical coupling with higher spatial scale
Statistical equivalence of representative volume elements
Multi-time scale behavior

## Slide 13: Limitations in Crystal Plasticity
#1 Missing Physics
Size invariance, Hall-Petch effect
Dislocation transport, starvation, and conservation laws
Slip bands, extrusions/intrusions, and persistent slip bands
Grain boundary transmission and energetics
#2 Lower Scale Effects
Dislocation core effects and key dislocation mechanisms
Accounting for measured initial dislocation density
Nanoscale voids, precipitates, microcracks, and inclusions
Solid solution hardening, compositional effects
#3 Evolution of Microstructural Input
Grain boundary sliding, coarsening, rotation, migration, and local misorientation
Nanoscale changes such as rafting, phase transformations, deformation twinning, and vacancy generation
#4 Fundamentals
Continuum assumption, separation of scales
Decoupling of elastic and plastic constitutive behavior
Orowan’s equation and Schmid behavior
Infinitesimal deformation and strain measures
#6 Extreme Values
Multi-junctions and field localizations are critical
Confidence in discretization and solver near extremes
Nonlocal length scales
#5 Boundary Conditions
Periodicity, self-consistency
Concurrent or hierarchical coupling with higher spatial scale
Statistical equivalence of representative volume elements
Multi-time scale behavior
#7 Computational Cost
>1,000 grains requires supercomputing
CPU and GPU parallelization add user/developer complexity
Global and constitutive time integration accuracy/stability thresholds
#8 Workflow Efficiency
Software integration
Reproducibility is nontrivial
Constitutive relation development requires competence in tensor analysis
Towards the end goal of crack initiation and microstructurally small crack growth
Fatigue indicator parameter-based approaches or explicit crack modeling are typically dependent on crystal plasticity
However, there is a complex interaction of assumptions and limitations in crystal plasticity
#8 Workflow Efficiency
Software integration
Reproducibility is nontrivial
Constitutive relation development requires competence in tensor analysis

## Slide 14: Limitations in Crystal Plasticity
So how can this space be navigated?
Simple and complex community benchmarks / challenge problems
#1 Missing Physics
Size invariance, Hall-Petch effect
Dislocation transport, starvation, and conservation laws
Slip bands, extrusions/intrusions, and persistent slip bands
Grain boundary transmission and energetics
#2 Lower Scale Effects
Dislocation core effects and key dislocation mechanisms
Accounting for measured initial dislocation density
Nanoscale voids, precipitates, microcracks, and inclusions
Solid solution hardening, compositional effects
#3 Evolution of Microstructural Input
Grain boundary sliding, coarsening, rotation, migration, and local misorientation
Nanoscale changes such as rafting, phase transformations, deformation twinning, and vacancy generation
#4 Fundamentals
Continuum assumption, separation of scales
Decoupling of elastic and plastic constitutive behavior
Orowan’s equation and Schmid behavior
Infinitesimal deformation and strain measures
#6 Extreme Values
Multi-junctions and field localizations are critical
Confidence in discretization and solver near extremes
Nonlocal length scales
#5 Boundary Conditions
Periodicity, self-consistency
Concurrent or hierarchical coupling with higher spatial scale
Statistical equivalence of representative volume elements
Multi-time scale behavior
#7 Computational Cost
>1,000 grains requires supercomputing
CPU and GPU parallelization add user/developer complexity
Global and constitutive time integration accuracy/stability thresholds
#8 Workflow Efficiency
Software integration
Reproducibility is nontrivial
Constitutive relation development requires competence in tensor analysis

## Slide 15: Crystal Plasticity and Q&C
Entry Points
Limitations
Trust
(1)
(2)
(3)
Why is crystal plasticity not playing a significant role in Q&C?

## Slide 16: Calibration and Validation of Crystal Plasticity
Common Calibration and Validation Methods
Bulk and mesoscale polycrystalline testing
Single crystal testing
In-situ loading with digital image correlation or high energy diffraction microscopy
Micropillar and nanoindentation experiments
Lower scale modeling
Common Calibration and Validation Challenges
Measuring relevant quantities at relevant length and time scales
Many model parameters difficult to decouple experimentally
By adding model complexity without corresponding experimental measurement, typically physics-based principles and interpretations are deteriorated, and model generalizability is lost.

## Slide 17: National Institute of Standards and Technology (NIST) Additive Manufacturing Benchmarks 2022
[1] Kafka et al. IMMI (2023) 12:196–209
Elastic modulus group predictions [1]
Logarithmic strain (yy)
111
101
100
Loading direction
500 μm
Finite element mesh
Global strain applied: 20%
-0.2
-0.1
0.0
101
111
100
Inverse pole figure map of EBSD scan
Error ~ 40%
Prediction
Measurement
Submitted tensile metric predictions for the
“Subcontinuum Mesoscale Tensile Challenge”

## Slide 18: Air Force Research Laboratory (AFRL) Additive Manufacturing 2020 Modeling Challenge
x10-3
Stress-strain curve
Tensile
coupon
Serial-sectioned
microstructure
28 “challenge” grains
515 μm
500 μm
Error < 2%
ff-HEDM: Far-field High-energy X-Ray diffraction microscopy
Elastic modulus predictions
3D microstructure of Inconel 625 provided
Grain-average elastic strains predicted at “challenge” grains

## Slide 19: Influence of Subsurface Microstructure
Z
Y
X
25.6 µm
25.6 µm
Open-source 3D dataset[1] of serial-sectioned Ti-6Al-4V alloy
Material produced via electron beam powder-bed fusion
Microstructure volume: 256 x 256 x 140 voxels
Voxel size: 0.1 x 0.1 x 0.1 μm
Surface strains from full 3D model
Surface strains from full “2.5D” model
[1]DeMott et al. Mendeley Data, V1, doi: 10.17632/c5x7ckcfsp.1
Percentage error in surface strains
Relative Error
in (%)

## Slide 20: Crystal Plasticity and Q&C
Entry Points
Limitations
Trust
(1)
(2)
(3)
Why is crystal plasticity not playing a significant role in Q&C?

## Slide 21: Computational Materials-Informed Qualification and Certification of Additively Manufactured (AM) Flight Hardware
Goal: Change the Paradigm for Qualification and Certification (Q&C)
Develop a computational materials-informed ecosystem for quantifying sources of variability in performance of additively manufactured metallic materials through integrated multi-scale, multi-physics simulation, characterization and monitoring
Process
Structure
Property / Performance
Porosity
5 mm
Location-specific properties
Small deviations
in process conditions
Potentially large variation in fatigue performance

## Slide 22: Structure-Property Calibration Workflow for AM Inconel 718
Microstructure
Loading Amplitude
Cycles to Initiation
106
102
103
104
105
X-ray computed tomography
Porosity characterization
Fast Fourier Transform (FFT) crystal plasticity
with GPU support and auto-differentiation
Fatigue indicator parameter based lifing
with porosity
In-situ load stage[1]
Grain-scale strain fields
AM Specimens[1]
Subscale ASTM E8
RoboMet[1]
Subsurface investigation
[1]Image Credit: Lopamudra Das, Andy Newman, Sang-Hyon Chu

## Slide 23: Platform for Prototyping Computational Materials for Q&C
PSP-UQ
Integrated Process-Structure-Property, Uncertainty Quantification Framework
Focus on model integration for calibration/validation and uncertainty quantification
Simplicity and ease of use
Integration of physical and computational capabilities within an AM data platform
Data model + database + data processing + registration
Computational
Physical
TRUST-AM
Trust and Reliability through Unified Simulation and Testing for Additive Manufacturing

## Slide 24: Conclusions
The number of decision points, assumptions, and limitations in a typical crystal plasticity workflow are vast.
Community benchmarks for mesoscale models are a good idea.
Entry points for crystal plasticity to impact Q&C exist but need maturation.
  Connecting to fracture mechanics is a promising avenue, especially cycles to crack initiation.
Characterization and prediction must work hand in hand, ideally in 3D.
Modeling Limitations
Missing Physics
Lower Scale Effects
Evolution of Microstructural Input
Fundamentals
Boundary Conditions
Extreme Values
Computational Cost
Workflow Efficiency
This work was supported by the NASA Aeronautics Research Mission Directorate (ARMD) Transformational Tools and Technologies (TTT) project
Acknowledgements
Contact : george.r.weber@nasa.gov