## Slide 1
Manufacturing of Aircraft Structures Using Composite Tailoring Techniques
Alana M. Cardona1, Erin K. Anderson1, Lauren Simmons1, Richard A. Larson1, Brian H. Mason1, and Jacob Tury2
NASA Langley Research Center, Hampton, VA
1Structural Mechanics and Concepts Branch
2Manufacturing Applications Branch
May 19-22, 2025
Indianapolis, IN

## Slide 2: Alana Cardona
Alana Cardona is an aerospace engineer who has been at NASA Langley Research Center in the Structures and Materials group since 2017. She is a subject matter expert in automated fiber placement, composite design, programming, and manufacturing. Additionally, she specializes in nonlinear analysis of composite materials, namely damage progression of thermoset prepreg materials and stitched, resin infused materials. She is currently the Deputy Integration Manager at the Integrated Structural Assembly of Advanced Composites (ISAAC) facility.

## Slide 3: Outline
Introduction
Manufacturing
  Integral Stiffener Research, Applications
  Tow-Steering Research, Applications
Advanced Curing Methods
Conclusions and Future Work

## Slide 4: Introduction
Motivation:
Aerospace industry seeking lightweight, fuel-efficient designs that maintain the strength and damage tolerance required for safe flight
  Advanced Air Transport Technology (AATT) project, Transonic Truss-Braced Wing (TTBW) concept
  Increased efficiency within commercial, single-aisle aircraft
  Nontraditional means to reduce weight, including integrating composite techniques into wing cover panels to reduce or remove metallic parts
Wing
Jury strut
Main strut

## Slide 5: Introduction
Objective:
Develop and demonstrate advanced composite tailoring techniques that can reduce weight and meet the strength requirements for flight certification
  Structural Wing Experiment Evaluating Truss-bracing, 15-Foot (SWEET-15)
  Wing cover panels contain tailored composite designs
  Wing is supported externally by a stitched resin-infused main strut
  Manufacturing and pre-assembly at Langley Research Center, then tested at Armstrong Flight Research Center in the Flight Loads Laboratory

## Slide 6: Automated Fiber Placement
Automated fiber placement (AFP) at NASA Langley Research Center
  Integrated Structural Assembly of Advanced Composites (ISAAC) facility
Places up to sixteen 6.4-mm (¼-in.) composite prepreg tows in multiple courses that make up a ply
Multiple plies create a full laminate
Spools
Heater
Roller
ISAAC robot
AFP head
Prepreg spools
Placement surface

## Slide 7: Integral Stiffener Research
Integral stiffener created by adding additional tows in select locations interleaved between skin plies
  Interleaving reduces likelihood of stiffener separation from skin
  Stiffener widths, stagger, and heights investigated
None
1.59 mm
(1/16 in.)
3.18 mm
(1/8 in.)
Vertical wall
Skin
Tapered wall
Skin
Interleaved stiffener plies
Acreage plies

## Slide 8: Integral Stiffener Research
Defect reduction
  Bridging reduced with staggered stiffeners compared to vertical wall
  Fewer stiffener plies between each skin ply
  Four-tow stiffener width provides better stiffening impacts and more gradual tapered edge
  Regular debulking to reduce compounding bridging effects
Bridging
3.18-mm stagger
No stagger
Pre-Debulk
Post-Debulk

## Slide 9: Integral Stiffener Applications
Total skin thickness optimized before adding integral stiffener
Differences between optimization and final laminate based on manufacturing ease and reliability
Panels programmed and manufactured at ISAAC with extra trim area
Inboard
Outboard
Inboard
Outboard
40 plies
36 plies
46 plies
16 plies
Number of plies
Initial design, unstiffened without ply drops
Final design, stiffened with ply drops

## Slide 10: Tow-Steering Research
Three different legacy designs with various extents of tow steering
  Straight fiber, lightly steered, and aggressively steered
Tested under compressive load
  Aggressively steered panels had 20% lower weight and 35.6% higher buckling load
Automated Tool for Steered COmposite Optimizable Laminates (ATSCOOL)
  Investigate more optimal tailoring of steered fiber laminates

## Slide 11: Tow-Steering Applications
Initial skin sizing optimized again, then select straight fiber plies replaced with steered plies with intentional gaps
Panels programmed and manufactured with extra trim area
Inboard
Outboard
Inboard
Outboard
36 plies
16 plies
20 plies
20 plies
Number of plies
Initial design, without tow steering
Final design, with tow steering

## Slide 12: Advanced Curing Methods
All panels thermoset composite prepreg designed for autoclave cure cycle
Flat inboard panels placed on invar tool, angled outboard panels on foam tool then invar tool
Cured under vacuum with silicone caul over top of panel
Heat/pressure cycle between 107-177 °C (225-350 °F) at 690 KPa (100 psi)
Notes: This cycle consisted of evacuating atmosphere from the vacuum bag via a vacuum pump and ramp heating the autoclave to 107 °C (225 °F) while increasing the pressure to 690 KPa (100 psi) gauge pressure. This pressure and temperature were held before further ramping the temperature to 177 °C (350 °F) and holding this next temperature and pressure for the remainder of the cure cycle. Subsequent cool down and pressure release occurred per workshop best practices.

## Slide 13: “Flat” Panel Cure
Integrally stiffened and tow-steered composite panels susceptible to warping
  Nonsymmetric coefficient of thermal expansion (CTE) distribution across the thickness
  Varying location of the neutral bending axis
Two-part silicone caul material used to match varying outer mold line surface and create flat outer surface for cure

## Slide 14: Tapered Height Cure
Outboard panels have inflection point and were not flat
Nonuniform caul surface, but heavy enough to act as a pressure intensifier even in thinnest caul regions
Final part dimensions drawn on (silver) for post-cure trim
Tapered angle change
Foam tooling

## Slide 15: Conclusions
Objective was to explore multiple advanced composite manufacturing concepts for integration into a complex truss-braced wing assembly
Full test article advances the state of the art of stitched resin infused composites, integrally stiffened composites, and tow-steered composites
Manufacturing applications can be used for many composite structures that benefit from fiber tailoring, lightweight structures, and increased strength and buckling requirements

## Slide 16: Future Work
Test to take place Fall 2025 at Armstrong Flight Research Center
  Plan to display capabilities of fiber optic strain sensing (FOSS) system for strain and damage mapping
Current best practices for AFP at the ISAAC facility continue to push the boundaries and advance capabilities for composite manufacturing
3.05 meters (10 feet)

## Slide 17: Questions?