## Slide 1: Digital Image Correlation Applications at NASA Langley Research Center (1990 to 2025)
David S. Dawicke
Analytical Services and Materials, inc.
May 7, 2025
Workshop on Novel and Emerging Uses of Sensor Technology in Mechanical, Fatigue, and Fracture Testing

## Slide 2: NASA LaRC James H. Starnes Structures Lab, B1148
Load Frame Test Machines
Focus on large static and combined load tests
~ 40 Load Frames: 5,000 lbs. to 1,000,000 lbs.
Environmental chambers: −320 to 600°F
Combined Loads Test System (COLTS)
  Combined pressure, axial, torsion, shear loading
  Test articles as large as 15 by 40 ft.
B1148
1M lbs. Load Frame
Backstop
COLTS

## Slide 3: NASA LaRC Fatigue and Fracture Lab, B1205
Load Frame Test Machines
Focus on sub-component and material level tests
Environmental Chambers: −320 to 600°F
Load Frames: 5,000 to 400,000 lbs.
Cyclic and static loading
B1205
3-Point Bend Composite Fatigue Crack Growth
Fracture
Sub-component Level Testing

## Slide 4: Other NASA and non-NASA Facilities Supported
-
-
NASA MSFC
NASA WSTF
Lockheed-Denver (NASA JPL)
Cimarron-Huntsville (NASA LaRC)
NASA JPL
NASA AFRC

## Slide 5: LaRC B1148/B1205 DIC Team
Dave Dawicke 1993 (really 2004) to present
Patrick McNeill 2009 to 2012
Nate Gardner 2012 to 2021
Michael McNeill 2015 to present
Matlock Mennu 2021 to 2024
Jasmine Knowles 2024 to present
Many high school, undergraduate, and graduate student lab interns

## Slide 6: 1990’s – “What are all these dots for?”
  2D digital image correlation (DIC) for crack tip opening angle (CTOA)
  3D DIC for fracture of large panels

## Slide 7: 2D DIC for Measuring Crack Tip Opening Angle (1993)
Crack Tip Strain Fields
Da = 0.80 mm
Da = 2.55 mm

## Slide 8: 3D DIC for Structural Deformations and Strains (~1996) J. D. Helm, M. A. Sutton, and S. R. McNeill
u-Displacements
v-Displacements
w-Displacements
x, u
z, w
y, v
29 kN
58 kN
116 kN
3D DIC Measurements
Finite Element Results

## Slide 9: 2000’s – Getting our Feet Wet
  Composite panel buckling and delamination
  Composite overwrapped pressure vessel (COPV) testing
  Large structure tests
  Cryogenic tests
  Test/model correlation
  Boundary conditions

## Slide 10: Composite Testing (2004 – 2008)
Load
(lbs)
D v-Displacement at 0.4 inches
(inch)
0.4 inch
Load
Displacement
D
Frame 396
Frame 397
Frame 716
Frame 717

## Slide 11: Shell Buckling Knockdown Factor (SBKF) (2007 – 2015)
Load Lines
Load Introduction
Cylinder
Load Introduction
Cylinder
Test
Article
70 ft
20 ft
20 ft
20 ft
10 ft

## Slide 12: SBKD Large Test Camera Placement at NASA MSFC
Six (6) external 3-D camera systems
  Full circumferential coverage
  Minimum amount of overlap between adjacent systems: ~ 15° (Considering correlated areas)
  Locations determined by where systems could be mounted to part of the building structure
Top view of 3-D DIC system layout
DIC System
Sys7 - NW
Sys6 - N
Sys5 - NE
Sys2 - SW
Sys3 - SE
Sys4 - E

## Slide 13: SBKF Data Visualization
Panel
G
Panel
H
Panel
A
Panel
B
Panel
G
Panel
H
Panel
A
Panel
B
VIC-3D Method of Stitching Multiple Camera Systems
Unwrapped cylinder with all systems plotted
[cylindrical coordinates]
Limited to 3-D plot and Cartesian coordinates only
ASTM Committees E08 on Fatigue and Fracture and E28 on Mechanical Testing

## Slide 14: 2010’s – Have Cameras, Will Travel
  Frangible joint explosive tests (ultra high-speed > 1,000,000 fps)
  Mars 2020 rover heat shield & rover wheel
  Composite wing
  More COPVs
  Wind tunnel testing (high-speed > 5,000 fps)
  More test/model correlation
  Grain orientation strain localization

## Slide 15: Frangible Joint (FJ) Explosive Tests (2014 – 2018)
Kirana (4 cameras)
  Resolution: 924 x 768
  Speed used: 1,000,000 to 5,000,000 fps
  Number of images: 180
Shimadzu HPV-X (4 cameras)
  Resolution: 400 x 250
  Speed used: 500,000 to 2,000,000 fps
  Number of images: 128
Photron SA-Z (2 cameras)
  Resolution: 256 x 128
  Speed used: 300,000 fps
  Number of images: >500
Notch
Confined
Explosive

## Slide 16: Example of FJ DIC (2,000,000 fps)
The contours identify constant values of out-of-plane displacement (w)

## Slide 17: Example of FJ DIC (2,000,000 fps), shown in 3D
The contours identify constant values of out-of-plane displacement (w)

## Slide 18: Comparison of Independent Measurement Methods
PDV: Photon Doppler Velocimetry
- Laser-based point velocity measurement technique
- PDV data acquisition rate < 0.5 msec
- PDV data acquisition time > 1,000 msec
- Laser point within the 3D DIC AOI
- DIC data extracted at the same location as the PDV laser point

## Slide 19: Passive Aeroelastic Tailored (PAT) Wing Test (2017)
Problem:
A full-scale composite wing (>40 feet) was tested in bending
Wing deformations needed for validation of structural analyses and composite designs
The rigidity of the boundary conditions was a concern, so characterization of support fixtures was required
Goals:
Quantify the wing deformations during upward and downward bending
Quantify the support fixtures to establish the boundary conditions for the structural analyses
Top View of Wing

## Slide 20: Top View Displacement (Rigid Body Motion Removed)
w-disp
(inch)
3
0
Side A – Trailing Edge
Side B – Leading Edge
ASTM Committees E08 on Fatigue and Fracture and E28 on Mechanical Testing

## Slide 21: Fixture Movement
w-disp
(inch)
0.5
0.0

## Slide 22: Damage Tolerance Testing of a Large Grain Material (2017 – 2019)
Problem:
A fracture critical space vehicle structure was found to have a large gradient in grain size (<0.001 inch to >0.2 inch) over a small area
Damage tolerance qualification was required to be demonstrated by test
The concerns:
  Tensile tests revealed large scatter in material properties
  The mismatch of adjacent large grains could create strain localization
  The location of the crack for damage tolerance testing is critical
Solution:
Use DIC to identify regions of strain localization to guide the placement of the fatigue crack
Etched Coupon
Back Surface
Front Surface

## Slide 23: Strain Localization & Grain Structure
Axial Strain
(%)
2
1

## Slide 24: Mars 2020 Rover Heat Shield (2018)
Problem:
The Mars 2020 rover heat shield (flight hardware) is required to have a ground proof test to 120% of the entry, descent, and landing loads
The first test performed in 2018 and the strain during loading was monitored with strain gages, but a fracture occurred away from the strain gages
The heat shield was redesigned for testing in 2019
A failure of the second proof test would likely cause a 2-year delay in the launch
Goals:
Perform full-field characterization of the entire heat shield in real-time during the proof test loading to prevent fracture by identifying any regions of elevated strain
Characterize the full-field strain distribution for validation of structural models
Space.com article from April 28, 2018

## Slide 25: DIC Setup
Hardware/Software:
Three pairs of cameras (every 120 degrees)
  30MP AVT cameras 50mm lenses
  Overlapping areas of interest (AOI)
Cameras mounted on 80/20 supported by ladders
Hardware-synced systems
VIC3D-8TM with RealTime
Aperture, exposure time, and lighting optimized
DIC Configuration
AOI ~ 176 inch by 117 inch
Pixel Resolution ~ 36 pixels/inch
Speckle Size ~ 0.1 inch (printed on vinyl)
Subset Size 29 pixels and Step Size 7 pixels
Standoff Distance ~ 15 feet
Camera Angle ~ 22-degrees
Calibration grid: 12x9 70mm
Issues
Travel logistics (i.e., make sure we have everything we need)
Flight hardware (i.e., surface must be returned to pristine condition and not damage during testing)
Real-time monitoring (i.e., ~1 second refresh) during loading
High strain resolution (< 100 microstrain)
Limited floor space

## Slide 26: Stitched DIC and Analysis Predictions at a Constant Pressure
TBD\
System 3
System 2
System 1
DIC Minimum Principal Strains
Analysis Minimum Principal Strains

## Slide 27: Mars 2020 Rover Heat Shield Findings and Ramifications
The Mars 2020 Heat Shield passed the 120% qualification test without fracture or strains that exceed prediction limits
The DIC strain and displacement measurements were in good agreement with independent point measurements
Full-field strain measurements were extracted at finite element analysis nodal locations for direct comparison with predictions

## Slide 28: Ascent Cover Separation System Test (2019)

## Slide 29: 2020’s – DIC Becomes Routine
  Residual strains due to welds
  More COPVs
  More frangible joints
  More test/model correlations
  Explosive tests

## Slide 30: Hypergolic Engine Pressure Spike Simulation (2022)
Hypergolic engines experience pressure spikes/transients that present structural/material design, qualification, and operational concerns
Goal: characterize the material response during the initial pressure impact, expected response:
  Impulse duration ~ 4 to 8 msec.
  Response duration < 250 msec.
  Out-of-plane displacements < 0.25 inch
  Out-of-plane velocities < 5000 inches/sec.
  Strains < 50,000 microstrain
Goal: characterization of test conditions
  Measurement of the out-of-plane displacement
  Test/analysis correlation requires a detailed understanding of the boundary conditions
  Flanges could deform (elastically and plastically) during testing
  Detection of gas escape between flange and coupon
Outer
Flange
Inner
Flange
Disk Coupon

## Slide 31
Computational Fluid Dynamics Modeling of Detonation Tube
Animation of static pressure on cut-plane through center of tube
Pressure Transducer
(Camera Trigger)
Flanges and Disk Coupon
Burst Disk
ASTM Committees E08 on Fatigue and Fracture and E28 on Mechanical Testing

## Slide 32
DIC System
Two Shimadzu HPV-X cameras
  Synced images at 2,000,000 to 500,000 frames per second
  400x250 pixels
  128 images
  Triggered ~4 to 10 msec. before impulse arrival
Flash lamp
  Triggered ~115 msec. before impulse arrival
  800-msec. duration
ASTM Committees E08 on Fatigue and Fracture and E28 on Mechanical Testing

## Slide 33
3D View
(Rigid Body Motion Removed)
2D View
(Rigid Body Motion Removed)
w
(inch)
0
0.15
DIC Displacement Measurements
ASTM Committees E08 on Fatigue and Fracture and E28 on Mechanical Testing

## Slide 34
Why Boundary Conditions are Important
3D View
2D View
w
(inch)
0
0.025
ASTM Committees E08 on Fatigue and Fracture and E28 on Mechanical Testing

## Slide 35
Gas Escaping Between Flange and Disk
ASTM Committees E08 on Fatigue and Fracture and E28 on Mechanical Testing

## Slide 36: Lessons Learned
Anticipate what is needed to be measured in addition to what is requested
Boundary conditions are critical
Follow the iDICs best practice guide for reporting results (https://www.idics.org/guide/)

## Slide 37: Contact Information
David S. Dawicke
Senior Scientist
Analytical Services and Material, Inc.
107 Research Dr.
Hampton, VA 23666
dave@asm-usa.com