## Slide 1: Ablative Material Fracture with Peridynamics
July 22, 2025
Andrew P. Santos, Lauren J. Abbott, Justin B. Haskins
Thermal Protection Materials Branch, NASA Ames Research Center, Moffett Field, CA, USA
18th US National Congress on Computational Mechanics
Chicago, IL, USA

## Slide 2: A Heat Shield for Every Mission
2
Schematic of entry process. Credits: NASA
Heat shields, thermal protection systems (TPS) provide:
thermal protection
help slow down vehicles during entry
mechanical strength
Mission’s trajectory and entry environments set the thermal and mechanical requirements
TPS composite materials have a wide range of microstructures and properties.
For TPS: One size does not fit all!

## Slide 3: Thermal Protection Systems (TPS) Types
Light, porous, low thermal conductivity, non-ablative, fibrous, ceramic.
Deployables
Reusables
Shuttle era HRSI LI-900 tile. NASA
Ablators
X-37b with TUFROC wing leading edge. NASA
Great for entry from low-earth orbit and backshells

## Slide 4: Thermal Protection Systems (TPS) Types
Deployables
Reusables
Ablators
3D TPS woven with carbon fibers in an
umbrella-type design
Hypersonic Inflatable Aerodynamic Decelerator uses donut/torus shaped balloons
Great for slowing down
Adept in the Arc Jet. NASA
Adept deploying. NASA
LOFTID deployment before entry. NASA
LOFTID entry. NASA

## Slide 5: Thermal Protection Systems (TPS) Types
D Ellerby et al, MS&T, 2019 • A Vanaerschot et al, Composite Structures, 2017, 173, 44-52
Infused Fiber Networks
Avcoat, PICA, SIRCA
Lower density
Deployables
Reusables
Weaves
HEEET, 3MDCP, 3D-MAT, Carbon-carbon
Higher density for more extreme entry
Ablators
SEM of fractured PICA
Full infused weave demonstration unit
Infused 3D weave microstructure
Artemis I Avcoat heat shield. NASA
Agrawal, Chavez-Garcia, J. Spacecraft Rockets, (4) 50, 2013

## Slide 6: Ablative TPS Mass Loss
Libben, et al (2019)
Designed
Manufacturing impurity and damage
Impacts from Micrometeoroid and Orbital Debris
Entry-induced
  Ablation, large deformation and heating
Anomalous
PICA ablating in the ArcJet. NASA
Ablation
Spallation
Impact of a woven TPS
Avcoat fracture in ArcJet. NASA

## Slide 7: Goal
7
Ultimate goal:
Predict anomalous mass loss and fracture of different TPS from manufacturing, impacts and entry.
This work’s goal:
Simulate room temperature fracture of PICA due to tension and impact. Motivated by (1) manufacturing and sourcing changes to material properties, and (2) MMOD impact.

## Slide 8: Phenolic Impregnated Carbon Ablator (PICA)
Developed in the 1980s at NASA Ames TSM
Low density, high porosity, robust
Efficient ablator
Can be manufactured into a
  single piece
  multi-tiled heat shield
The PICA manufacturing process. NASA
Missions
Stardust (1999)
Mars Science Laboratory (rovers) (2011)
OSIRIS-Rex (2023)
Mars 2020
OSIRIS-Rex (2023)
SpaceX’s Dragon (2010-current)
Dragonfly (2028)

## Slide 9: Phenolic Impregnated Carbon Ablator (PICA)
charred PICA
virgin PICA
FiberForm
The PICA manufacturing process. NASA
Microstructure:
Fiborous
Anisotropic
Very porous
Modelling challenges:
Manufacturing, heat-shield scale design and microstructure affect fracture
Entry is a thermo-chemical-mechanical coupled response
Agrawal, Chavez-Garcia, J. Spacecraft Rockets, (4) 50, 2013

## Slide 10: TPS Modeling
Peridynamics
fracture during impact
microscale
mesoscale
Thermal conductivity
Mesoscale-resolved
Continuum Material Response
heat shield recession
Explicit-fiber Discrete element
3D weave relaxation
Bonded-particle model
phenolic resin model
Meshed methods are crucial for TPS design sizing
Particle-based methods bridge the scale gap to model chemistry, microstructure and damage

## Slide 11: Structure-Resolved Approaches
Liu, D. et al. Comput. Mater. Sci. 2025, 251, 113731.
Schill, W. et al. Carbon 2021, 171, 376–384.
Analyze thermal conductivity, orientation, mass loss with PuMA (NASA ARC-TSM)
Semeraro F et al. Comput. Mater Sci. 2020.
Ferguson JC et al. Carbon. 2016
Ringel B et al. AIAA Scitech. 2024
Semeraro F et al. Computational Materials Science. 2021
Fraile Izquierdo S et al. AIAA SciTech. 2016
Simulate constituents with cohesive law fiber and bonded-particle models (NASA ARC-TSM)
Solve continuum mechanics with FEM, LPM, peridynamics, phase field, etc. (NASA ARC-TSM)

## Slide 12: Continuum-scale Approaches
R. Fu, S. McDaniel, et al., in AIAA Scitech 2021 Forum (2021).
J. B. E. Meurisse, et al., Aerosp. Sci. Technol. 76, 497 (2018).
C. Luo and P. E. DesJardin, Compos. Sci. Technol. 67, 1475 (2007).
Zhang, Y.; Behera, D.; Madenci, E. Eng. Comput. 40 343-365 (2023).
Material Response:
Heat shield recession
FVM, FEM:
Crack path in a square mesh
Peridynamics:
Fracture of charring ablator
Material response codes model many entry-relevant physics on the continuum scale
Finite element methods accurately capture solid mechanics but require apriori knowledge of cracks
Peridynamics is a mesh-free solid mechanics technique, developed for fracture by inherently capturing discontinuities, and successfully modeled TPS
Distributed material properties can be used to capture microstructural effects

## Slide 13: FiberForm, virgin/charred PICA Fracture Experiments
Agrawal, Chavez-Garcia, J. Spacecraft Rockets, (4) 50, 2013
57 mm
3.8 mm
9.7 mm
1.3 mm
Experimental fracture test setup and sample dimensions.
Experimental fracture of FiberForm, virgin and char PICA by Agrawal & Chavez-Garcia.
The phenolic resin strengthens and stiffens the material.
Tensile stress-strain (σ-ε) of notched samples of FiberForm, virgin PICA and charred PICA.

## Slide 14: SEM at the Crack Tip
Agrawal, Chavez-Garcia, J. Spacecraft Rockets, (4) 50, 2013
Post-test SEM helps identify what drives fracture:
fiber pullout in FiberForm
phenolic matrix-dense regions in PICA
charred PICA
SEM at crack tip.
virgin PICA
FiberForm

## Slide 15: Tensile fracture in peridynamics
Agrawal, Chavez-Garcia, J. Spacecraft Rockets, (4) 50, 2013
Panerai, F. et al. IJHMT 2016, 101, 267–273
Methodology
Energy released rate calculated from fracture toughness
LAMMPS fix deform (affine motion perpendicular to crack)
state-basted, linear peridynamic solid:
Strain rate: 10-4 m/s
Lgrid , grid spacing [mm], Horizon: 3 Lgrid
Property | FiberForm | Virgin | Char
Density [kg/m3] | 183.6 | O(100) | O(100)
K, Bulk Modulus [GPa] | 0.081 | 0.11 | 0.2
G, Shear Modulus [GPa] | 0.045 | 0.06 | 0.11
Tensile Strength [MPa] | 0.44 | 1.1 | 0.78
Gic, E. release rate [J/m2] | 2.64x103 | 3.81x103 | 3.08x103
PICA properties used in Peridynamics simulations
Peridynamics notched specimen configuration. Different spacings and horizons were used.

## Slide 16: Tensile fracture of FiberForm in peridynamics
Peridynamics simulation of notched sample. Color correspond to damage (0: purple; 1: yellow).
Crack at notch starts at 0.005% strain and propagates at 0.02% strain. Frames are from the central slice of the material.
=10-4m/s, dt=5x10-8s, dl=0.3 mm.
(right) Fracture path in virgin PICA.

## Slide 17
Ballistic Impact Testing
Ballistic testing of HEEET-RL (denser version of 3MDCP) has been performed for MSR
Testing performed on the recession layer (RL) of HEEET at the White Sands Hypervelocity Impact Testing facility
Impact testing is limited to the use of impactors that are heavier and slower than expected MMODs
 | Ballistic impact | MMOD
impactor material | aluminum or nylon | Regolith type
diameter | 1-5 mm | ~0.05 mm
velocity | 7 km/s | 25 km/s
Libben, et al (2019); Haskins et al. (2025)
Woven material specimen with multiple impacts
MMOD mass-velocity heat map

## Slide 18
Ballistic Impact Testing
Peridynamics was able to reproduce “fingers” in the crack propagation of the weaves, when the yarn-scale mesostructure is incorporated
The microstructure dominates in PICA, a fiber network. So we are going to keep with the homogenous model.
 | Ballistic impact | MMOD
impactor material | aluminum or nylon | Regolith type
diameter | 1-5 mm | ~0.05 mm
velocity | 7 km/s | 25 km/s
Libben, et al (2019); Haskins et al. (2025)
Infused weave; 7 km/s; nylon impactor
Impacted resin (light) woven fiber (dark) peridynamics configuration; (LAMMPS)

## Slide 19: MMOD impact of FiberForm
Peridynamics simulation of a disk sample. Color correspond to damage (0: blue; 1: red).
=10-4m/s, dt=5x10-8s, dl=0.3 mm center slice.
Methodology
Use predicted MMOD velocity (25000 m/s) and density (2200 kg/m3)
Peridigm, state-based, linear peridynamic solid

## Slide 20
Next steps
Validate fracture behavior against experiments
Apply homogenous/microstructure-agnostic technique to other TPS
Reproduce PICA failure mechanisms in bonded particle models
Still early days for applying fracture simulations to TPS
We are looking to get engagement and complimentary techniques from the computational mechanics and fracture communities:
Fracture experiments of TPS at high T and T gradients
Models appropriate for highly-porous materials
Coupling gas flow and pressure with mechanics
Questions?

## Slide 21: Tensile fracture in peridynamics
Peridynamics simulation of notched sample. Transparency and color correspond to damage (from 0, transparent and purple, to 1, opaque and yellow.
Experimental fracture of FiberForm, virgin and char PICA by Agrawal & Chavez-Garcia
FiberForm mechanism: fiber pullout
Virgin and Char PICA mechanism: phenolic matrix porosity
Intensity factor is a crucial parameter for fracture mechanics simulations
=10-3m/s, dt=5x10-8s, dl=0.3 mm
=10-2m/s, dt=1x10-7s, dl=0.5 mm
=10-5m/s, dt=5x10-8s, dl=0.3 mm

## Slide 22: FiberForm, virgin/charred PICA Fracture Experiments
Agrawal, Chavez-Garcia, J. Spacecraft Rockets, (4) 50, 2013
57 mm
3.8 mm
9.7 mm
1.3 mm
Experimental fracture test setup and sample dimensions.
Experimental fracture of FiberForm, virgin and char PICA by Agrawal & Chavez-Garcia. They measured stress-strain curves and fracture toughness.
Tensile stress-strain (σ-ε) of unnotched (solid) and notched (dashed) samples of FiberForm, virgin PICA and charred PICA.
unnotched
notched

## Slide 23: Tensile fracture in peridynamics
+Agrawal, Chavez-Garcia, J. Spacecraft Rockets, (4) 50, 2013
Panerai, F. et al. IJHMT 2016, 101, 267–273
Methodlogy
Energy released rate calculated from fracture toughness
LAMMPS fix deform (affine motion perpendicular to crack)
state-basted, linear peridynamic solid:
Strain rate: 10-4 m/s
Lgrid , grid spacing [mm], Horizon: 3 Lgrid
Peridynamics notched specimen configuraton. Different spacings and horizons were used.
state-basted, Linear peridynamic solid:
influence function ω, reference state 𝑥, weighted volume m, dilatation θ, deviatoric extension state ed, bulk modulus K and normalized shear modulus ⍺.