## Slide 1: Shortcomings of Li-Ion Cell Visual Screening Methods
By: Ruth Young CACI International (United States),
Eric Darcy Johnson Space Center,
Aidan Byrne Amentum
Trade names and trademarks are used in this report for identification only. Their usage does not constitute an official endorsement, either expressed or implied, by the National Aeronautics and Space Administration

## Slide 2: Acknowledgements
Eric Darcy (JSC)
Thank you for the mentorship and technical guidance
Frank Samonski (JSC)
JSC Materials Analysis Lab for the support
Symmetry Resources Inc
For continued cell testing support
Ovidio Oliveras (JSC) & Aidan Byrne (JSC)
Thank you for providing the CT scan support and expertise

## Slide 3: Outline
JSC Cell Strategic Reserve (CSR)
  Models in the Reserve
  Screening Process
  Lifecycle Quality
Shortcomings of Visual Screening Methods
  Example: Leaking Electrolyte on Passing Visual Inspection Cell
Capacity vs Voltage Balance in Cell Screening
Forward Work

## Slide 4: NASA’s Cell Strategic Reserve
What is it?
  A reserve of Li-Ion cells screened via NASA standards
  Several cell designs are kept in stock with various key performance advantages (ex: High Energy vs High Power)
    Molicel M35A
    Molicel P28B
    Samsung 30Q
    LG M36

## Slide 5: High Energy Cell Designs
LG INR18650 M36
Previous heritage
Superior resistance to side wall rupture
At C/10 and room temperature
  270 Wh/kg, 710 Wh/L
  ACR is 23.9 mohms
  DCR is 29.8 mohms
70k lot (Nov 2020) delivered in Apr to JSC
Molicel INR18650-M35A
Little previous heritage
Same manufacturer of ICR18650J, primary power for > 25 EVAs
Superior extreme cold performance
  214 Wh/kg at C/20 and -20ºC
At C/10 and room temperature
  277 Wh/kg, 725 Wh/L
  ACR is 24.4 mohms
  DCR is 32.5 mohms
120k lot (Feb 2021) delivered in Apr to JSC

## Slide 6: High Power Cell Designs
Samsung INR18650-30Q
Previous heritage
  X-57 Electric Airplane
  Safe high power battery demo
At 3C and room temperature
  2483 W/kg, 206.9 Wh/kg
  6340 W/L, 528.1 Wh/L
  12.4 mohm ACR
  26.2 mohm DCR
60k lot (Mar 2021) delivered in June to JSC
Molicel INR18650-P28B
No previous heritage
Not mass produced due to 2nd cathode tab
At 3C and room temperature
  2528 W/kg, 202.3 Wh/kg
  6376 W/L, 510.3 Wh/L
  9.2 mohm ACR
  22.3 mohm DCR
  5.5% waste heat – Smallest of the 4 cell types
60k lot (Aug 2021) delivered in Oct to JSC

## Slide 7: The Importance of Cell Screening
Manufacturer Cell Acceptance Standards
vs
NASA Flight Battery Cell Acceptance Standards
  Human Rated Missions
  JSC20793

## Slide 8: Cell Process Flow Chart
Cell Design Surveillance
~10 cell designs/yr
Deeper Dive into best 5 designs
Buy large cell lot
Basic performance verification
Longer cycling & special performance,
TR calorimetry, ISC trigger cells,
Audit production line
w/ traceability to manufacturer
Initial Lot Assessment
EP-WI-036B, N2
270 unscreened cells for SWR
Fail
Lot Acceptance
EP-WI-033A
N2 - 5 cells
EDU Batteries
Fail
Reject Lot or Cells
Cell Screening (Mission)
EP-WI-037A
SDR test or OCV (>1yr after BOD)
Qualification & Mission Batteries
Reject Lot or Cells
Fail
Receiving Inspection, EP-WI-035
Inventory Cell Lot
Cell Screening for EDU
EP-WI-037A
Pass
Pass
Pass
Pass
Pass

## Slide 9: Initial Lot Assessment (ILA)
EP-WI-036 Specification for Initial Lot Assessment of Commercial Lithium-ion Cells Lots
Determine if cell lot (N1 lot size) is worthy before proceeding with an expensive lot acceptance testing - Quick & less expensive (8 weeks, ~$150k)
  Expected performance in accordance with cell surveillance results
  Acceptable lot uniformity of performance, particularly charge retention
  Acceptable quality of manufacture
  Propensity to sidewall rupture during TR (90% confidence level, 5% MOE)
Verify cell design has not changed
Assess manufacture performance and quality
Self-Discharge Rate (SDR)
AC Impedance
Closed Circuit Voltage (CCV)
Open-Circuit Voltage (OCV)
Sample size N2 at 90% confidence level with a 5% margin of error (MOE) (for N1 = 70k cells, N2 = 270 cells) or one cell from each box, whichever is greater
Visual Inspection
Capacity Cycling, C-Rate with DC Resistance
Dimensional
Mass
Report Data and Statistics. May reject, but not accept!
Computed Tomography (CT) on 5 cells
Destructive Physical Analysis (DPA) on 5 cells
Side Wall Rupture (SWR) Characterization
Report Results & Data
May reject, but not accept
Capacity Cycling, C/20 Rate with dQ/dV, 3 cells
Pull another N2 cells from Inventory
N2- 8 cells for Lot Acceptance testing
Identification
Report Results, Data and Statistics
Electrochemical Impedance Spectroscopy (EIS) 3 cells
Report Results, Data and Statistics
n ≥ 3
n ≥ 5

## Slide 10: Lot Acceptance Testing
7.0 Cell Seal Integrity
n ≥ 13 (3 control)
8.0 CT/DPA
n ≥ 9
14.0 Archive (spare cells) n ≥ 12
10.0 Performance Calorimetry
n ≥ 3
N ≥ 3
n ≥ 13
N ≥ 3
n ≥ 23
n ≥ 12
n ≥ 30
n ≥ 53
n ≥ 36
Design, Performance, Quality, and Safety Testing
N ≥ 173 cells
12.0 TR Calorimetry
n ≥ 20
6.0 Post Environment Capacity Performance
n ≥ 30 Repeat 4.0
13.0 Life Tests (53 cells)
13.2 Calendar Life n ≥ 45
13.1 Cycle Life
n ≥ 8
(n also depends on battery configuration)
4.0 Capacity Performance n ≥ 30
4.1 Charge, 27 cells
3 temperatures, 3 rates
4.2 Discharge, 27 cells
3 temperatures, 3 rates
4.3 OCV vs. SoC, 3 cells
C/20 rate at ambient T&P
5.0 Environmental Tests n ≥ 30
15 cells 100% SoC, 15 cells 0% SoC at each Environment
5.1 Thermal Cycling
5.2 Pressure Cycling
5.3 Random Vibe.
N ≥ 6
n ≥ 6
N ≥ 3
n ≥ 42
11.0 Electrical Abuse n ≥ 36
11.1 Overcharge
n ≥ 12
11.2 External Short Circuit n ≥ 24
9.0 Cell Enclosure Vent/Burst Pressure n ≥ 12, or n ≥ 18 for bottom vent
9.1 Vent Pressure n ≥ 6
Fully discharged C/10
9.2 Burst Pressure n ≥ 6
Fully discharged C/10
9.1 Vent Pressure n ≥ 6
Bottom vent, Fully discharged
Notes: 11.2 elinimatred. 36 for 11.1 and 11.3

## Slide 11: Lifecycle Quality of Cells
Source: “JPL Testing of COTS Li-ion Cells - NASA Strategic Reserve (10-06-2025) Rev. B”
Notes: 1 year is 6000 cycles approx. (16 cycles a day, 90 min orbit around earth), station wanted 10 year cycle life (60,000 cycles)
Lithium plating in LEO cycles bc you are always charging or discharging – no chance for lithium to dissolve back into solution – leads to build up of dendrites
***add in some sort of take home 1 liner – what is capacity degradation over 17500 cycles

## Slide 12: Calendar Life Testing

## Slide 13: Overall Stats on 68,000 Screened 18650 Cells
Visual Inspection (8.17%)
  Scratches
  Corrosion
  Dents
  Cuts
  Discoloration on weld surfaces
Electrical (3.61%)
  Majority due to outlying OCV
Dimensional/Mass (0.24%)
Chart: 68,000 Screened Cells
| Passing | Visual | Dimensional | Electrical
 | 60202 | 5592 | 166 | 2468

## Slide 14: Defects
Chart: LG M36 Rejects
| Passing | Visual | Dimensional | Electrical
 | 43791 | 2815 | 109 | 1394
Chart: Moli P28B Rejects
| Passing | Visual | Dimensional | Electrical
 | 6072 | 1715 | 17 | 133
Chart: Samsung 30Q Rejects
| Passing | Visual | Dimensional | Electrical
 | 2263 | 235 | 4 | 78
Chart: Moli M35A Rejects
| Passing | Visual | Dimensional | Electrical
 | 8076 | 827 | 36 | 863
Chart: 68,000 Screened Cells
| Passing | Visual | Dimensional | Electrical
 | 60202 | 5592 | 166 | 2468

## Slide 15: Current Shortcomings of Visual Screening
Throughput capacity for high volume
Subjectivity of analysis

## Slide 16: Example – Leaking P28B

## Slide 17: Screening for Leaks
EP-WI-037B

## Slide 18: Screening for Leaks
EP-WI-037B

## Slide 19: Leaking P28B Cell
Calendar life Testing year 3
  Lost 15% capacity
  DCR changed +178%
  Lost 1.2g electrolyte
Tried various optical methods to find a hole -> unsuccessful
  Profilometer
  Stereomicroscopy
  CT scan
  Dye penetrant analysis

## Slide 20
Stereomicroscope Examination
7x
100x
Inclined
Inclined

## Slide 21: Screening for Leaks
EP-WI-037B
Electrolyte salts leaves colorful residue
Crack may have grown in 3rd year upon capacity cycling
  54µm crack width at 0% SoC
  Measured the same at 100% SoC

## Slide 22: SOC Impact
OCV = 3.101V
OCV = 4.109V
At 4.11V during 300mA charging, rise of ΔT = 9°C terminating charge. No odor, no discoloration

## Slide 23: CT Scanning/Profilometer

## Slide 24: Examination of Header

## Slide 25: Leaking P28B Cell
Leak detector
  Inficon’s ELT3000 Plus
    Instrument has a leak threshold of 1.8x10-6 mbar*L/s for DMC (Dimethyl Carbonate)
  Measured Leakage Rates:
    7.3x10-5 mbar*L/s
    1.8x10-4 mbar*L/s
  Capped bottom and top of cell in various configurations, isolated leak to top of cell

## Slide 26: Leaking P28B Cell

## Slide 27: Post Inficon Scans

## Slide 28: Post Inficon Scans

## Slide 29: Capacity vs Voltage Balance

## Slide 30: Cell Screening -> Pack Preparation
1. Determine cell capacity and DCR uniformity
  Reject ± 3σ outlying cells
  Reject lot with insufficient uniformity
    > 5% for 6σ/μ for capacity
    > 15% for 6σ/μ for DCR
3. Verification of cell balance
  Assemble screened (passing) cells into 8S battery strings
  Charge each string fully without any cell balancing
  Measure OCV balance at 100% SoC
2. Prepare cells for battery assembly with highest OCV balance at the top of charge

## Slide 31: Voltage Balance Determination
CC/CV charge to 4.2V and C/50 taper current
Discharge fully to minimum voltage
  With DCR pulse at 50% SoC
  Screen for cell capacity and DCR from this discharge
  This leaves the cells in voltage balance but not in capacity balance
Partial recharge with 10% capacity input (~10% SoC)
  Constant current input with Ah termination

## Slide 32: Capacity Balance Determination
Discharge to minimum voltage
Full CC/CV charge to 4.2V and C/50 taper current
  With DCR pulse at 50% SoC
  Screen for cell capacity from the charge cycle
  Cells balanced at the TOP of cell CAPACITY
Discharge to 10% SoC based on capacity output
  Remove the same Ah from each cell

## Slide 33: Voltage vs Capacity Balance Impact on 8S Battery String at Top of Charge
Chart: OCVs after Voltage Balanced Cell Screening
| 0 | 30 | 60
260A-R08-C08(V) | 4.201 | 4.1871 | 4.1839
115A-R04-C05(V) | 4.2115 | 4.1973 | 4.1943
253B-R07-C06(V) | 4.1972 | 4.1836 | 4.1809
290A-R03-C08(V) | 4.2002 | 4.1866 | 4.1837
269A-R10-C10(V) | 4.1913 | 4.1777 | 4.1748
104A-R08-C07(V) | 4.1759 | 4.1629 | 4.1602
253A-R10-C01(V) | 4.1962 | 4.1823 | 4.1794
244A-R03-C02(V) | 4.2095 | 4.195 | 4.1913
Chart: Cell OCVs after Capacity Balanced Cell Screening
| 0 | 30 | 60
290B-R07-C03 (V) | 4.1996 | 4.1855 | 4.1822
266B-R04-C01(V) | 4.1976 | 4.184 | 4.181
253B-R03-C02(V) | 4.1967 | 4.1831 | 4.1798
115B-R03-C09(V) | 4.1973 | 4.1837 | 4.1806
104B-R03-C09(V) | 4.199 | 4.1853 | 4.1824
253A-R07-C04(V) | 4.198 | 4.1843 | 4.1811
100B-R07-C02(V) | 4.1971 | 4.1832 | 4.1804
244B-R05-C05(V) | 4.198 | 4.1841 | 4.1808

## Slide 34: Voltage vs Capacity Balance Impact on 8S Battery String at Top of Charge
Chart: Cell OCVs after Capacity Balanced Cell Screening
| 0 | 30 | 60
290B-R07-C03 (V) | 4.1996 | 4.1855 | 4.1822
266B-R04-C01(V) | 4.1976 | 4.184 | 4.181
253B-R03-C02(V) | 4.1967 | 4.1831 | 4.1798
115B-R03-C09(V) | 4.1973 | 4.1837 | 4.1806
104B-R03-C09(V) | 4.199 | 4.1853 | 4.1824
253A-R07-C04(V) | 4.198 | 4.1843 | 4.1811
100B-R07-C02(V) | 4.1971 | 4.1832 | 4.1804
244B-R05-C05(V) | 4.198 | 4.1841 | 4.1808
Capacity balancing the SOC of cells during cell screening improves OCV uniformity from 30 to 3 mV in an 8S string.

## Slide 35: Conclusions & Forward Work
Measured Leak Rate of Cell
  7.3x10-5 mbar*L/s
  1.8x10-4 mbar*L/s
Forward work to analyze protruding material
How do we improve on screening of cells to account for shortcomings of visual screening methods?
  Why did it only impact year 3 of the calendar life test?
    Screen LAT/ILA cells using leak rate instrument
    Crack doesn’t grow with SOC
    No visual confirmation of deformity until several cycles under vacuum with leak detector
  Industry standards for leak detection are under development
    Inficon’s leak rate instrument using quadropole mass spectroscopy tuned for DMC solvent in Li-ion electrolyte is a leading method
  Economic trade – Cost of screening every cell going into a battery using leak detector
Notes: People that do nothing besides remove shrink wrap vs residual gas analysis of every single cell (we used to do the latter, got no failures, and it was expensive)

## Slide 36: End

## Slide 37: Overall Cell Screen Stats

## Slide 38: High Energy Cell Designs
LG INR18650 M36
Previous heritage
  250 µm can wall
  Safety fully characterized by JSC
  Multiple variations beam tested in FTRC
  3 batches of ISCD trigger cells delivered to JSC
At C/10 and room temperature
  270 Wh/kg, 710 Wh/L
  ACR is 23.9 mohms
  DCR is 29.8 mohms
70k lot (Nov 2020) delivered in Apr to JSC
Molicel INR18650-M35A
Little previous heritage
  Same manufacturer of ICR18650J, primary power for > 25 EVAs
  Superior extreme cold performance
    214 Wh/kg at C/20 and -20ºC
  Multiple batches of ISCD trigger cells delivered to JSC
At C/10 and room temperature
  277 Wh/kg, 725 Wh/L
  ACR is 24.4 mohms
  DCR is 32.5 mohms
120k lot (Feb 2021) delivered in Apr to JSC

## Slide 39: Our High Power Cell Designs
Samsung INR18650-30Q
Previous heritage
  X-57 Electric Airplane
  Safe high power battery demo
At 3C and room temperature
  2483 W/kg, 206.9 Wh/kg
  6340 W/L, 528.1 Wh/L
  12.4 mohm ACR
  26.2 mohm DCR
  8.3% average waste heat
60k lot (Mar 2021) delivered in June to JSC
Molicel INR18650-P28B
No previous heritage
Not mass produced due to 2nd cathode tab
At 3C and room temperature
  2528 W/kg, 202.3 Wh/kg
  6376 W/L, 510.3 Wh/L
  9.2 mohm ACR
  22.3 mohm DCR
  5.5% waste heat
60k lot (Aug 2021) delivered in Oct to JSC

## Slide 40: LG M36
Electrical (2.90%)
  Majority due to outlying OCV, CAMX CST, or ACZ
Dimensional/Mass (0.23%)
Visual Inspection (5.85%)
  Corrosion
  Scratches
  Pitting
  Dents
Chart: LG M36 Rejects
| Passing | Visual | Dimensional | Electrical
 | 43791 | 2815 | 109 | 1394

## Slide 41: Molicel M35A
Chart: Moli M35A Rejects
| Passing | Visual | Dimensional | Electrical
 | 8076 | 827 | 36 | 863
Electrical (8.80%)
  Majority due to outlying OCV or CAMX CST
Dimensional/Mass (0.37%)
Visual Inspection (8.44%)
  Dents
  Scratches
  Corrosion
  Discoloration on weld surfaces

## Slide 42: Molicel P28B
Electrical (1.68%)
  Majority due to outlying DC
Dimensional/Mass (0.21%)
Visual Inspection (21.61%)
  Scratches
  Corrosion
  Dents
  Discoloration
Chart: Moli P28B Rejects
| Passing | Visual | Dimensional | Electrical
 | 6072 | 1715 | 17 | 133

## Slide 43: Samsung 30Q
Electrical (3.02%)
  Majority due to outlying CCV
Dimensional/Mass (0.16%)
Visual Inspection (9.11%)
  Dents
  Corrosion
  Scratches
  Cuts
Chart: Samsung 30Q Rejects
| Passing | Visual | Dimensional | Electrical
 | 2263 | 235 | 4 | 78

## Slide 44: Backup Slides

## Slide 45: Samsung 53G1 Cell
Samsung makes OCV data out to 4 decimal places available via QR code on each cell can

## Slide 46: P28B dOCV Screen Data

## Slide 47: Example - dOCV Cell Screening

## Slide 48: P28B Pre-Screen OCV Check
Chart: Cell Number
+3s | 3.5608 | 3.5608
-3s | 3.5231 | 3.5231
+2s | 3.5545 | 3.5545
-2s | 3.5294 | 3.5294
+1s | 3.5482 | 3.5482
-1s | 3.5357 | 3.5357
+ns | 3.5608 | 3.5608
-ns | 3.5231 | 3.5231
OCV measurement 1 yr after fabrication
  Want 10-12 mV range for +/-3 sigma, NOT 40 mV
Trimodal distribution seen, decided a dOCV measurement was needed to pass or fail cells on OCV

## Slide 49: Motivation for dOCV Screen
Going from 95% to 65% SOC is ~200mV delta
  Some NASA programs will condemn battery at a 50 mV un-balance (~7% SOC drop)
  Spacesuit battery is NO GO for EVA if there is >20 mV difference
Want to screen out potential latent internal cell shorts
  Some latent defects could be showing very subtle OCV decays
Chart from “Capacity Performance, Environmental Test, and Post Environment Capacity Performance for Lot Assessment Test Report” done by PCTest for JSC CSR P28B Cell Lot

## Slide 50: dOCV Process
Manufacturer (Manf. SN)
OCV check #1 (Manf. SN)
OCV check #2 (Manf. SN)
Screened Data Used to determine passing dOCV for a given lot
Passing Cells reserved for upgrade for use on flight
CT image sample of passing/failing cells
9 mo. Gap where cells are shipped back to CSR
Rest of screening (Manf. SN -> Screen SN)
Pre-OCV Check at JSC
Measured to 4 dec places, 18-bit (or better) resolution meter
Notes: Question: Is there a correlation between dOCV failure and a bridging defect between anode and cathode visible by CT?
Hypothesis: Presence of high density (metallic) “bright spots” in JR could bridge anode to cathode causing internal shorts and leading to dOCV failures

## Slide 51: Key Cell Finding #1 – Anode Buckling
Overlap of inner wind anode tab with start of cathode layer leading to severe buckling angle of anode
  Buckling appears in both PASS and FAIL dOCV cells
FAILING Cell
Passing Cell

## Slide 52: Key Cell Finding #2 – Delamination/Cathode Damage
Severe buckling on failing cells showed a trend of delaminating graphite from anode
Severe dOCV fails tend to have delamination at start of cathode at the inner wind
FAILING Cells

## Slide 53: Follow- Up Work
Follow up dOCV measurements taken 10 weeks later
  Failing cells:
    Monthly voltage decrease: 2.4 mV/mo
    Avg dOCV: 5.8 mV
  Passing cells:
    Monthly voltage decrease: 1.1 mV/mo
    Avg dOCV: 2.7 mV
Clear difference in passing vs failing cells
  DPA not performed due to CT defects occurring in center of JR
Notes: Pull in darcy slides, add in slide with CT scan of leaking cell
With cell at 60 SOC and 10 deg C there should be very little degradation
Key messages,
There is a cell reserve you can tak advantage of
Cells are ~5 years old but there is cal life testing / cycle life testing that shows that cells are good (can pull from the JPL presentation for this one)
Add in this years cal life testing
Grab the ILA/LAT flow plots from dec 24 reserve presentation so that you can put it in the appendix
Slides 191-196 from cell review chart deck for showing how many cells get rejected
Store cells in freezer under 30 SOC for best longevity
Stopping at capacity determination vs stopping at a voltage determination
Voltage determination is worse, when you go put cells in series you charge to same # of Ah and then they are not as balanced
Capacity determination, balance all cells at the top of the charge cycle (balance at same voltage for 100 SOC)
  30 -> 0 -> 100 -> 90 to compare charge capacity
1 year is 6000 cycles approx. (16 cycles a day, 90 min orbit around earth), station wanted 10 year cycle life (60,000 cycles)
Lithium plating in LEO cycles bc you are always charging or discharging – no chance for lithium to dissolve back into solution – leads to build up of dendrites

## Slide 54: Pre-dOCV Screen Data
Arrow denotes failing Cell Selection for CT scans

## Slide 55: Pre-dOCV Screen Data
 | # | % Entire Lot (56,552)
Total Rejects | 679 | 1.2%
Low Rejects | 27 | 0.0477%
High Rejects | 447 | 0.79%
No Data Rejects | 205 | 0.362%
Note 2 cells from failing negative range were picked, range not shown on graph
Ignored low rejects that were not negative
Failing Cell Selection for CT scans
Passing Cell Selection for CT scan

## Slide 56: Passing Cell dOCV Data
Removal of 3σ outliers until 3σ range is stable and 6σ% approaches 0
  -/+3σ = 5.34 / 11.96 mV
  6σ% = 0.765%
*Ignored low rejects that were not negative

## Slide 57: Raw Data*
*Graph does not show extreme outliers as it causes the rest of the graph to be unreadable

## Slide 58: Raw Data*
*Graph does not show extreme outliers as it causes the rest of the graph to be unreadable

## Slide 59: Raw Data ALL - Sorted