## Slide 1
Development of an Additively Manufactured Subscale Secondary Sealed Container for the NASA FROSTE Project
Melissa Forton, Collin Adair, Blake Hyla, Ryan Anderson , & Joseph Sims – Quadrus Corporation
Joe Sanford – NASA FROSTE Project Manager
Distribution Statement A. Approved for public release: distribution is unlimited.

## Slide 2: Overview of FROSTE Work
FROSTE Program Overview
Quadrus Corporation’s Role
Secondary Sealed Container Overview
Phase Change Material Tank
  Design Overview
  Internal Lattice Details
  Manufacturing Process
  Powder Removal
Conclusions & Future Work

## Slide 3: FROSTE Program Overview
Frozen Return of Sample to Earth (FROSTE)
  Targeting cryogenic Sample Return from the Permanently Shadowed Regions (PSRs) at the lunar south pole
    Temperatures in PSRs are below 100K
    FROSTE will maintain 100K temperature from sample collection to splashdown on Earth to preserve trapped volatiles in the sample
  Goal is to bring back 50kg of samples
  Return vessel has been designated as the Secondary Sealed Container (SSC)
Preliminary SSC Design Concept
“THE COOLEST PROJECT AT NASA”

## Slide 4
Quadrus Corporation’s Role in FROSTE
Quadrus Corporation’s Role
Design and build a proof-of-concept subscale Secondary Sealed Container (SSC)
Demonstrate the overall capabilities of Additive Manufacturing in for the FROSTE program
Laser Powder Bed Fusion
Colibrium Additive M2 Series 4 Plus
Design Requirements
Temperatures down to 80K
Vacuum to 10-7 Torr

## Slide 5
Manufacturing Considerations
Colibrium Additive M2 Series 4 Build Volume: 250mm x 250mm x 378mm
Build Plate Footprint
250mm x 250mm outline
2-inch Build Plate

## Slide 6
Secondary Sealed Container Terms
Primary Container Assemblies
Phase Change Material Tank Assembly
Outer Container Assembly
*MLI not shown

## Slide 7: Secondary Sealed Container Overview
Outer Container Assembly
Primary Container Assembly
PCM Tank Assembly

## Slide 8: SSC Assembly Details
PCM Tank Assembly rotates into position, and lock pins are inserted

## Slide 9: SSC Thermal Disconnect Method from Cryocoolers

## Slide 10: Phase Change Material Tank Design Features
Design Features
Monolithic, One-Piece Component
Phase Change Material: 2-Methylpentane or 2-Methylpentane with Acetone
Internal Lattice Structure to help evenly distribute thermal loads through the PCM
Fill, Drain, and Vent Ports
Integrated Thermocouple Tubes
Design for Solo and Assembled SSC Testing
  Direct Connect Thermal Straps
  Pads for SSC Thermal Plunger Assembly

## Slide 11: Scalmalloy
Scalmalloy
Started life as 5000 series
  Aluminum alloy with Magnesium
Added Scandium to make Weldable
Unique Bimodal Microstructure
  Equiaxed and Columnar Grains
Mechanical Properties
Slightly lower strength than 7075-T6
Equivalent Strength-to-Weight Ratio of Ti-6Al-4V
Quadrus AM Scalmalloy Properties
  Yield Strength = 69 ksi
  Ultimate Strength = 73 ksi
Thermal Properties
Thermal Conductivity @ RT = 95 W/m-K
Scalmalloy Micrograph

## Slide 12: Phase Change Material Tank
Anti-Rotation Feature
Thermocouple Channels (28)
Drain Port
Internal Volume filled with Lattice
Fill Port
Retaining Ring Grooves
Thermal Contact Surface (SSC Testing)
Thermocouples in groups of 4 at quarter, half, three quarter, and full height.
Thermal Contact Surface (PCM Tank Testing)
Vent Port

## Slide 13: PCM Tank Manufacturing Challenges
Challenges
Large overhang parallel to build plate
Powder removal
Surface finish on thermal pads and primary container slots
Thermocouple sizing
Overhand Surface (Blue)
Powder Drainage Pathways (Yellow Arrows)
Thermal Pads
Mini PCM Tank Build ( Pancake Build)
Thermocouple Sizing

## Slide 14: PCM Tank Lattice
Radial Octet Truss Lattice
20% Relative Density

## Slide 15: LPB-F Build Setup
STL File - 3DXpert
Slice Files - Materialise Magics 29
Colibrium Additive M2 Series 4 Plus
Dual 400W Lasers
Build Time Estimation – 11 days*
Should equal 100%

## Slide 16: Lattice File Estimation
Largest Part with Lattice Geometry to Date
Slice File Size = 19.1 GB (Typical Part Slice Files Size <300 MB)
Radial Octet Truss Lattice Generation Issue
Sections of lattice randomly missing
New Lattice Geometry - Cubic Octet Truss
20% Relative Density maintained, but cell size increased
Slice File Size 19.1 GB
Slice File Size 3.0 GB
Cell size was too small creating too much geometric complexity

## Slide 17: Updated PCM Tank
Colibrium Additive M2 Series 4 Plus
Dual 400W Lasers
Build Time Estimation
4 day 4 hrs

## Slide 18: PCM Tank Build Video
Total Build Time
4 day 19.5 hrs
Single Layer of Build at 3x Speed

## Slide 19: PCM Tank Pictures
Total Build Time
4 day 19.5 hrs

## Slide 20: Powder Removal
NASA MSFC Solukon Shaker Machine
Estimated Time to Remove Powder = 1 week

## Slide 21: Subscale Secondary Seal Container
iMLI not included
Part Type | Quantity
AM Parts | 22
Subtractive Parts | 4
G10 Insulator Parts | 12
Seals | 8
Swagelok Compression Fittings | 3
Fasteners, Pins, Springs, Retaining Rings | 43
Quick-Clamp High-Vaccum Fitting | 1
iMLI Component | 1
TOTAL PART COUNT | 94

## Slide 22
Build Layouts
22
Build 1
Build 2
Build 3
Build 4
Build 5
Build 6
≈ 4.5 Days
≈ 1.5 Days
≈ 0.5 Day
≈ 1 Day
≈ 2.5 Days
≈ 0.5 Day

## Slide 23: Conclusions—Future Work
PCM Tank
CTE Scan the PCM Tank to assess how well it built as compared to the CAD
Final Machine PCM Tank
Deliver to NASA MSFC for solo testing
SSC Assembly
5 More LPBF Builds
Final Machine Parts
Assembly
Deliver to NASA MSFC for SSC testing

## Slide 24: Acknowledgements
I would like to recognize and give special thanks to:
NASA MSFC for funding this effort
My Quadrus coworkers who helped with effort
iMLI not included

## Slide 25: Questions?
690 Discovery Dr NW Huntsville, AL 35806
256.327.3410 | QuadrusCorp.com
25

## Slide 26: Additional Slides

## Slide 27: Scalmalloy Skin and Core Scan Strategy
Skin and Core Scan Strategy
  Skin - Continuous Scan Strategy with 30-micron layers
    Thickness can be varied
    Scalmalloy uses a thickness of 1.0mm
  Core – Island Scan Strategy with 60-micron layers
    Allows core to cool a little bit between laser exposures
  Skin Power = ½ Core Power
  Better control over surface finish
  Faster production times
Skin
Core
1.0mm