## Slide 1
The Future of Electronics RESHAPED 2026
June 10, 2026
Cadré Francis
Electronics Lead In-Space Manufacturing - Advanced Space Technologies for Resilient Operations Space Systems Department, NASA Marshall Space Flight Center
In-Space Manufacturing of Electronics
nasa.gov | Approved for public release.

## Slide 2
Mission Motivation
03 / 0:00
Agenda
TRL Pathway
05 / 2:00
Additive Electronics in Microgravity
05 / 3:00
Microgravity Demonstrations
07 / 6:00
Program Structure
Partnerships
12 / 12:00
Q & A
13 / 14:00
Key Challenges
14 / 15:00
11 / 9:00
nasa.gov | Approved for public release.

## Slide 3
Why In-Space Manufacturing?
nasa.gov | Approved for public release.

## Slide 4
Development of in-space manufacturing of electronics capabilities for microgravity manufacturing of electronics, sensors, and semiconductors
  Primarily for Use on Earth
In-Space Manufacturing: Advanced Space Technologies for Resilient Operations
CO2 Sensor
Crew Health Wearable Wireless Sensor
Plant growth strain sensor
Why in-space electronics?
Long-duration missions need adaptable, repairable systems
Spares add mass & mission risk
On-demand manufacturing facilitates resilience and autonomy
Objective 2
Objective 1
ISM-ASTRO
Development of electronics, sensors, and semiconductors for in-space manufacturing
  Primarily for Use in Space
Electronics
Additive manufacturing of PCBs
Material properties in space
Electronics printers
Microelectronics and Sensors
Semiconductors
Energy/Power
nasa.gov | Approved for public release.

## Slide 5
nasa.gov | Approved for public release.

## Slide 6
Materials – related µg Impacts
nasa.gov | Approved for public release.

## Slide 7: ISM Electronics Technology Development Approach
Microgravity – Demonstrate
Lunar Habitat – Use
CLDs – Commercialize
Parabolic Flights - Test
Ground Development
Ground-based development and optimization of technologies.
High-throughput experiments for data and validation.
Enabling more infrastructure for experiments and future volume manufacturing.
Parabolic flight campaigns to reduce risk of microgravity manufacturing.
Working with ISS NL and multiple integration partners for microgravity demonstrations of semiconductor technologies.
nasa.gov | Approved for public release.
Notes: Standard approach taken by ODME is risk reduction with parabolic flights followed by an ISS demo to understand microgravity effects since data is limited for parabolic flights. Final Infusion is either surface or commercialize.

## Slide 8
Predictive Modeling
nasa.gov | Approved for public release.

## Slide 9
nasa.gov | Approved for public release.

## Slide 10
Multi-Layer Printing
  Filling vias between substrate layers to connect circuit layers.
  Printed crossovers using conductive and insulating inks.
Chip Integration
  Printed insulator to hold chips in place and fill moats (printed chambers).
  Printed interconnects over moats to component pads top of chips
  Developing technology to insert a wider range of components.
nasa.gov | Approved for public release.

## Slide 11
Parabolic Flights : Deposition Phenomena
Thin-Film
nasa.gov | Approved for public release.
Advanced Toolplate System
SmartPump modification was successful. No clogging or stiction issues were experienced during the flight.
Samples used to inform partner model being developed to better understand DIW-deposition in microgravity.
A Vertical Interconnect Access (Via) is a small hole used to connect different layers of a circuit.
Via-filling is a pivotal part of fabricating high-performance circuits.
Moat filling involves dispensing dielectric paste around embedded components.
Moat filling is required to evaluate component placing and device manufacturability in microgravity.
Via Filling
Moat Filling
Formulate and test inks in reduced gravity environments
  Inks include Ag, BaTiO3, ZnO, PDMS
Micro-structures of printed patterns results in denser structure with fewer pores
Silver loading can be increased from 35 % (at 1g) to 50 % (at mg) due to less agglomeration  8.1 times higher conductivity

## Slide 12
Chapter Breaks
nasa.gov | Approved for public release.

## Slide 13
Exploration & Science
NASA Exploration and Support "In Space for Space" development
ECLSS Sensors
Wearable sensors
Printed Power & Energy
Avionics
Logistics – spares and upgrades for missions
Commercialization
Support "In Space for Earth Applications" development
Semiconductors
Academic
University of Louisville
University of Alabama Huntsville
Appalachian State University
Auburn University
Boise State University
Georgia Institute of Technology
California Institute of Technology
Iowa State University
Florida A&M University
Oregon State University
West Virginia University
University of Louisville
University of Alabama Huntsville
Appalachian State University
Auburn University
Boise State University
Georgia Institute of Technology
California Institute of Technology
Iowa State University
Florida A&M University
Oregon State University
West Virginia University
NASA Centers
Marshall Space Flight Center
Ames Research Center
Johnson Space Center
Kennedy Space Center
Goddard Space Flight Center
Glenn Research Center
Armstrong Flight Research Center
Industry/Government
Redwire Space
Cornerstone Research Group
LambdaVision
Faraday Incorporated
Laboratory for Physical Sciences
Intel
Lockheed Martin
ThinkOrbital
Fujifilm
Axiom Space
ISS National Lab
Goeppert
NextFlex
nScrypt
Sciperio
Multi3D
Astral Materials
ISM Electronics Collaborations & Partnerships
nasa.gov | Approved for public release.