## Slide 1: Thermostructural Testing of PICA-D for NASA Planetary Science Missions
23rd International Planetary Probe Workshop June 22 – 26, 2026
Milad Mahzari, Keith Peterson, Matt Gasch, Suman Muppidi, Michael Wright
NASA Ames Research Center Derek Shannon, Jack Joyce, Nick Courtney
Lockheed Martin Inc.

## Slide 2: Introduction
PICA-D is the heatshield TPS material for NASA’s Dragonfly mission
  Domestic replacement for heritage PICA used on past NASA missions (Stardust, MSL, OSIRIS-Rex, M2020)
  Initial expectation was that PICA-D would behave similarly to PICA allowing the team to leverage testing by past programs
Subsequent data indicated a shift in some mechanical properties compared to PICA
  Higher in-plane tensile stiffness and thermal expansion
  Preliminary thermostructural analysis predicted thermally driven compressive failure of PICA-D
Thermostructural performance concerns spurred a significant verification program
  Analysis and test plans were presented at the 20th IPPW
  Collaboration with Mars Sample Retrieval Lander team
This talk provides an overview of testing and analysis efforts to verify PICA-D performance
Dragonfly Entry Vehicle
PICA-D Tiles & RTV Gap Filler
Mars2020 Tiled PICA Heatshield
In-Plane Thermal Expansion
IP Thermal Expansion (Char)
Temperature
Failure Strain
IP Tensile Strength
PICA-D vs PICA in IP Tension

## Slide 3: Overview Of Risk Mitigation Approach
PICA-D Mechanical Property Testing
FEM Analysis Informs flight margins, failure modes and test design
Thermostructural Verification Testing
Dragonfly and SRL adopted a four-pronged approach to address the PICA-D thermostructural risk and verify its performance
Maturing and Testing Backup TPS – Conformal PICA*
Peak Temperature Testing of PICA-D at Solar Tower
Bonded PICA-D Mechanical Tests at Lockheed Martin (cold, RT, hot)
Acreage PICA-D
Gap Filler, Flaws, Repairs
Mechanical Test of CPICA
Arcjet Test of CPICA
CPICA Infusion Demo at FMI
* Pursued only for SRL
Comprehensive Test Matrix Executed at Kratos
Restrained Thermal Growth Testing of Char PICA-D
Temperature
IP Compressive Stress
Softening above PICA-D processing temp

## Slide 4: Solar Tower Test Overview
Heliostat field focuses Sun’s energy on a test stand at the top of tower
Test coupon faces the heliostat field
Insulation materials protect test fixture, exposing PICA-D coupon to intense solar radiation
Vacuum chucks with different curvatures apply enforced deflection to 2-ft diameter PICA-D coupons generating mechanical stress
N2 flow minimizes carbon combustion in presence of atmospheric oxygen
Full field
Q1
Q2
Q3
Q4
Heat profile designed to achieve flight-like temperature gradient and char depth
Infrared camera used to verify peak surface temperature
Coupons with thermocouple plugs verified in-depth temperatures
TC Plug
The team developed a novel test method at Sandia’s solar tower facility that enabled combined thermal and mechanical testing of PICA-D coupons at scales large enough to generate flight-like stresses
Filtered HD camera used to monitor coupon performance

## Slide 5: Test Video – Credit: Jenna Boss (JPL)

## Slide 6: Thermostructural Test Entries
Test ID | Objective | Failure Modes | Date | Acreage Coupons | Feature Coupons
ST1 | Test Development & Risk Reduction | Biaxial IP Compression | 08/2023 | 2 | None
 |  |  | 09/2023 | 4 | None
 |  |  | 12/2023 | 2 | None
LHMEL | Alternate Facility Evaluation |  | 02/2024 | 2 | 2
ST2 | Flight Verification Acreage & Features |  | 09/2024 | 2 | 4
ST3 | Flight Verification Acreage & Features |  | 08/2025 | 1 2 shoulder | 5
ST4 | Flight Verification Shoulder & Features | TT Shear, TT Tension | 03/2026 | 2 | 4
Solar tower selected for flight verification due to LHMEL’s smaller coupons and non-uniform laser heating pattern
New Test Fixture for Shoulder Coupons
Feature coupons containing gap fillers, flaws and repair methods tested in addition to acreage coupons

## Slide 7: Closing Thoughts
Thermotructural performance of the PICA-D bonded to the heatshield structure has been verified through a combination of analysis and coupon testing
  PICA-D mechanical material properties are better understood than heritage PICA
  Many advancements have been made in analysis and testing methods compared to previous programs including the development of a novel test technique and procedures at solar tower facility for flight verification testing
The PICA-D Heatshield TPS design, including features and flaws, has proven to be robust and capable of achieving the Dragonfly mission to Titan
  Held “PICA-D thermostructural peer review” on June 9, 2026 where we showed test/analysis results to project stakeholders and external SMEs and got concurrence that the PICA-D tiled heatshield design is good for flight!
In future material development efforts and early proposal stages, more focus on characterizing residual risks as opposed to justifying a TRL level will help with identifying risk mitigation steps early and alleviate the kind of schedule pressure that the Dragonfly and SRL teams faced

## Slide 8: Acknowledgements
PICA-D thermostructural performance has been a key area of interest on both Dragonfly and SRL. Many engineers from NASA Ames, Lockheed Martin , APL, JPL, Sandia and Kratos have been involved in evaluating this issue and developing testing and mitigation strategies. The authors would like to acknowledge contributions/feedback/support from:
Questions?
NASA Ames Keith Peterson Matt Gasch Suman Muppidi Owen Nishioka Mike Wright Helen Hwang Jonathan Morgan Josh Monk Olivia Schroeder Hannah Alpert
JPL MSR SRL Charisse Chen Brandon Smith Ravi Prakash Erich Brandeau Dan Coatta Jason Ginn Marcus Lobbia Steve Sell
JHU APL Karen Kirby Wayne Dellinger Ken Hibbard
Lockheed Martin Derek Shannon Jack Joyce Nick Courtney Sam Preece Todd Arterburn
Sandia Ken Armijo Aaron Overacker Hayden Harper Luis Garcia
Kratos Bhavesh Patel Kelly Mccullers Rafael Gonzalez
Sacrifices were made!