## Slide 1
Ceramic Matrix Composite (CMC) Thermal Protection Systems (TPS) and Hot Structures for Hypersonic Vehicles
David E. Glass, Ph.D.
Senior Technologist, Advanced Structural / Thermal Systems
Applied Materials for Space & Hypersonics (AMSH)
NASA Langley Research Center, Hampton, VA 23681
Approved for Public Release
Thermal Protection Systems for Space Applications American Ceramic Society Course
NASA Johnson Space Center
August 6, 2026
Additional details can be found in AIAA-2008-2682

## Slide 2: Outline
Introduction
  Ceramic matrix composites (CMCs)
  Aerothermodynamic heating
  Thermal management
  Thermal protection systems (TPS) for rocket-launched vehicles
  TPS and hot structures for hypersonic vehicles
TPS and Hot Structures Components
Key Technical Challenges
Concluding Remarks

## Slide 3: What are Composites?
Boeing Dreamliner 787
Two or more constituents combined on macro scale
  Often comprises a matrix (binder) and reinforcement
Types of reinforcement
  Continuous or long fibers
    Unidirectional, woven, braided, or random architecture
  Random or short fibers
  Particulate, flakes, or fillers
Benefits
  Lightweight
  Tailorable to different applications
    Strength / stiffness
    Coefficient of thermal expansion (CTE)
    Hardness, fatigue life, damage tolerance
Common composite examples
  Reinforced concrete and masonry
  Composite wood such as plywood
  Polymer matrix composites (PMC)
  Ceramic matrix composites (CMC)
PMC versus metallic properties
B787 PMC fuselage
Credit: “N1015X Air Tahiti Nui Boeing 787-9 Dreamliner 26 " by New York-air licensed under CCA 4.0.
Credit: “Composite Bike (3665606309)" by Paul Hudson licensed under CCA 2.0.
PMC composite bicycle
Credit: “Spruce Plywood" by Bystander licensed under CCA 3.0.
Composite plywood

## Slide 4: Ceramic Matrix Composites (CMCs)
CMC = Ceramic (or carbon) fiber in a ceramic matrix
  Material nomenclature is “fiber/matrix”
Common examples
  Oxides: Oxide/alumina-silicate, oxide/alumina-mullite
  Carbides: SiC/SiC, C/SiC, C/C-SiC
  Carbon/carbon: C/C
Characteristics
      Moderate density
      High use temperature
      Chemical resilience
      Excellent mechanical capability
“Game changer” for high-temperature applications
Monolithic ceramic
CMC
Monolithic ceramic panel
CMC panel
180 mph
(290 km/hr)
180 mph
(290 km/hr)
Credit: GE Aerospace, used with permission
Environmental barrier coating (EBC) (possible)
Fiber: silicon carbide (SiC), carbon (C), oxide, etc.
Fiber-matrix interface coating (possible)
Matrix: SiC, C, oxide, etc.
Unidirectional fibers shown

## Slide 5: Perception of CMCs
Analogous to that of PMCs in the mid-1980s
Commonly viewed as promising, but…
  Too many problems, unknowns, and risks
  Immature manufacturing techniques
  Immature supply chain
  Exotic
  Complex to analyze and implement
  Too expensive and therefore unrealistic for “real-world structures”
Is this perception valid?
CMC brake discs, calipers, and pads are NOT complex, immature, or risky
Credit: J. Chenenko, used with permission

## Slide 6
Reality of CMCs
Offer increased efficiency and decreased complexity for elevated-temperature applications
  Viable predictive and design capabilities
  Proof of profitability in multiple industries
  An actively developing supply chain
  Technological advances/improvements in manufacturing
    Can be tailored to application
    Decreased costs with increased quality and throughput
  Analogous to PMC composites in the mid-80s – CMCs are poised for explosive growth…
Have reached an inflection point in maturation
Credit: "EBACE 2019, Le Grand-Saconnex (EB190671)" by Matti Blume licensed under CCA 4.0.
Passport engine oxide/oxide mixer and nozzle

## Slide 7: Cost Perceptions and Cost Realities of CMCs
CMCs have a reputation as too expensive
  Acquisition costs can cause hesitation in adoption of CMCs, even if life-cycle costs are reasonable
  Costs must be balanced against the drivers for CMCs
Business case for CMCs in aviation drove GE investment
Used by permission of GE Aerospace: Approved for external publication (July 2024)
Investment in industrialization for high-pull business cases improves future business cases
S.J. Lewis, “The use of carbon fibre composites on military aircraft,” Composites Manufacturing, Vol. 5 No. 2, 1994.
Credit: “British Aerospace EAP at the Farnborough Air Show, 1986" by Mean as custard licensed under CCA 3.0.
Credit: “Tennis Racket and Balls" by Vladsinger licensed under CCA 3.0.
PMC Business Case Evolution
1980’s to present
High
Sector Level of
Industrialization / Capitalization
Low
Cost may not be competitive
Business case for industrialization
Cost often competitive
Cost can be competitive
Demand / Pull for CMC Technology
Performance
Efficiency
Emissions
Environmental
Safety
Low
High
Funding
$40M US government funding
GE funding
2022
2016
> $1B GE funding

## Slide 8: CMCs Are Both Enablers and Benefit-Multipliers
CMCs enable new technologies and products
  Spacecraft, aircraft, defense, nuclear, and other power generation components are some currently identified examples
CMC implementation results in system benefits
  CMC components enable a system with lower weight, higher performance, higher efficiency and improved safety while decreasing overall complexity – a benefit-multiplier
Aerospace: new materials enable new vehicles
Credit: NASA
Credit: NASA

## Slide 9: CMC Sectors
CMCs are currently making in-roads in multiple key industrial sectors
Credit: "IRIS-T air-to-air-missile" by Owly K licensed under CCA 3.0.
Credit: “ORNL History (44684257470)" by ORNL History licensed under CCA 2.0.
Nuclear fuel rods
Rocket control vanes
Automotive
Energy
Defense
Aviation
Aircraft engine shrouds
Credit: "PCCB Brake Carrera GT" by Nrbelex licensed under CCA 3.0.
Brakes
Credit: General Atomics Electromagnetic Systems (GA-EMS), used with permission
Credit: “Space Rider mission” by ESA©ESA, ESA Standard License
Space and Hypersonics
ESA Space Rider

## Slide 10
Outline
Introduction
  Ceramic matrix composites (CMCs)
  Aerothermodynamic heating
  Thermal management
  TPS for rocket-launched vehicles
  TPS and hot structures for hypersonic vehicles
TPS and Hot Structures Components
Key Technical Challenges
Concluding Remarks

## Slide 11
Two Stage to Orbit (TSTO) Reference Vehicle
Altitude, kft
100
200
300
0
0
5
10
15
20
25
Mach Number
Dynamic pressure
2000 psf
500 psf
100 psf
Stage separation
1st stage return
to launch site
Rocket upper stage
Increased heating, f (V3)
M ~ kft/sec
100 kft ~ 30 km

## Slide 12
Heat Flux
Reference heating,
1-ft-diameter sphere
Heat flux, Btu/ft2-sec
Time, sec
Rocket boost
Heating ~ V3
Crew Exploration Vehicle (CEV) Low Earth Orbit (LEO)
Single Stage to Orbit (SSTO) Airbreather (AB)
Heat Load = Heat flux dt
t=0
tfinal
∫
100 Btu/ft2-sec ~ 113 W/cm2
100 W/cm2 ~ 88 Btu/ft2-sec

## Slide 13
Heat load, Btu/ft2
Heat Load
Heat load, Btu/ft2
Time, sec
Reference heating,
1-ft-diameter sphere

## Slide 14
Introduction
  Ceramic matrix composites (CMCs)
  Aerothermodynamic heating
  Thermal management
  TPS for rocket-launched vehicles
  TPS and hot structures for hypersonic vehicles
TPS and Hot Structures Components
Key Technical Challenges
Concluding Remarks
Outline

## Slide 15: TPS & Hot Structures
In the US, the term “TPS” is usually used to include
  Acreage TPS such as tiles, blankets, and ablators (manage the heat)
    Insulation
  Hot structures such as control surfaces, leading edges, and nose caps
    Multi-functional structures that carry structural loads at operating temperatures (handle the heat)
Europe and most of the rest of the world use the terms TPS & hot structures separately
Tile TPS
Hot-structure control surface
TPS & hot structures can perform very different functions and should be referred to separately
Insulator / ablator
Structure
Aeroshells
TPS
Hot structures
C/C is used for the entire spectrum

## Slide 16: C/C as a TPS and/or a Hot Structure
Genesis ablative TPS
Hot-structure
control surfaces
Insulator / ablator
Structure
Aeroshells
TPS
Hot structures
C/C is used for the entire spectrum
Building block (and often the C/C) is component dependent
Early building block metrics
Arc-jet test
Density
Early building block metrics
Mechanical properties at elevated temperature
HTV-2 ablative aeroshell hot-structure
Credit: DARPA
HTV: Hypersonic Technology Vehicle

## Slide 17
5000
4000
3000
2000
1000
Temp., °F
0
1
2
Apollo / CEV
Ablators
Insulation
Mercury
Hot structure
Insulation
Active cooling
SR-71
X-15
Exposure Time, hr
Heat sink
Hot structure
Shuttle Orbiter
SSTO
Flight Vehicle Thermal Management
Earl Thornton, “Thermal Structures for Aerospace Applications”, AIAA Press, 1996.
3000°F ~ 1650°C
Time limited
Not time limited

## Slide 18
Heat radiated away
  Maximize surface emissivity
Minimal heat conducted inward
Structure remains cool
Use: Moderate heat flux, short times
Orbiter
Passive: Insulated Structure
Structure
Insulation
Surface heating
Radiation
Conduction
High emissivity surface
Heat Flux
Time
Moderate
High
Time limited
Not time limited

## Slide 19
Heat Flux
Time
Moderate
High
Time limited
Not time limited
Heat radiated away
Heat absorbed by structure
Radiation
Surface heating
Conduction
Passive: Heat-Sink Structure
X-15
Structure

## Slide 20
Heat Flux
Time
Moderate
High
Time limited
Not time limited
Heat radiated away
Heat conducted inward
Structure operates hot
Surface heating
Radiation
Structure
Passive: Hot Structure
Control surface manufacturing demo
Conduction

## Slide 21
Heat Flux
Time
Moderate
High
Time limited
Not time limited
Heat transferred by working fluid
Heat radiated away
Structure operates hot
Semi-Passive: Heat Pipe
Notional leading edge
Working
fluid
Surface heating
Radiation
Structure

## Slide 22
Heat Flux
Time
Moderate
High
Time limited
Not time limited
Heat blocked by products of ablation (ablator consumed)
Heat absorbed by ablation
Structure remains cool
Surface heating
Air flow
Structure
Ablator
Semi-Passive: Ablation

## Slide 23
Heat transferred into coolant
Coolant heats up and carries heat away
Structure operates hot
Coolant flow
Surface heating
Radiation
Structure
Active: Convective Cooling
Heat Flux
Time
Moderate
High
Time limited
Not time limited
Space shuttle main engine

## Slide 24
Coolant injected into flow (upstream)
Thin, cool, “insulating” blanket
Structure operates hot
Surface heating
Coolant flow
Air flow
Structure
Active: Film Cooling
X-43
Heat Flux
Time
Moderate
High
Time limited
Not time limited

## Slide 25
Coolant injected into flow (porous structure)
Coolant decreases heat flux to structure
Structure operates hot
Surface heating
Coolant flow
Air flow
Thrust chamber
Active: Transpiration Cooling
Heat Flux
Time
Moderate
High
Time limited
Not time limited

## Slide 26
Introduction
  Ceramic matrix composites (CMCs)
  Aerothermodynamic heating
  Thermal management
  TPS for rocket-launched vehicles
  TPS and hot structures for hypersonic vehicles
TPS and Hot Structures Components
Key Technical Challenges
Concluding Remarks
Outline

## Slide 27
Conventional skin-stringer aluminum aircraft structure
Structural temperatures < 350°F (176°C)
Reusable surface insulation (RSI) tiles
Reusable blankets
Reinforced carbon/carbon (RCC) used for wing
leading edges and nose cap, T > 2300°F (1260°C)
Space Shuttle Orbiter
Tile
Blanket
RCC Leading Edge

## Slide 28
Elevon - insulated with ceramic tile
C/C leading edge, fillet, and fin tip
Carbon/carbon (C/C)
nose cap, chin,
and skirt
Windward body -
Inco 617/MA754
metallic TPS (1333 panels)
Leeward aeroshell composite/blanket (17 panels)
Canted fin -
metallic (windward)
blanket (leeward)
X-33 Thermal Protection System
Similar to Orbiter TPS except metallic TPS on windward surface

## Slide 29
Introduction
  Ceramic matrix composites (CMCs)
  Aerothermodynamic heating
  Thermal management
  TPS for rocket-launched vehicles
  TPS and hot structures for hypersonic vehicles
TPS and Hot Structures Components
Key Technical Challenges
Concluding Remarks
Outline

## Slide 30
TPS and Hot Structures
Propulsion
Aerodynamics and Aerothermodynamics
Airbreathing Hypersonic Vehicles
Vehicle propulsion, airframe, and aerothermodynamics are highly integrated

## Slide 31
  Accelerate only
  Usually vertical launch
  Get out quick
  Low dynamic pressure
  Accelerate and cruise in atmosphere
  Typically horizontal launch
  High dynamic pressure
Rocket
Airbreather
Rocket vs. Airbreather: Flight in Atmosphere

## Slide 32
  High drag not a problem on ascent
  Desirable on descent for deceleration
  Optimize for low drag
  Thin, slender body, low thickness-to-chord ratio
Rocket
Airbreather
Rocket vs. Airbreather: Drag

## Slide 33: Key Point: Drag Reduction
Reentry vehicles (most of our prior experience) want drag to reduce velocity during reentry
Vehicles flying in the atmosphere must minimize drag during atmospheric flight
  Surface and cross-section
Hot structure is the preferred approach (rather than TPS over cold structure)
  Thin cross sections are required – hot structure is more volumetrically efficient
Credit: DARPA

## Slide 34
Weight Critical
  Structural mass fraction ~10% of gross take off weight (GTOW)
Volume Critical
  Volume impacts drag
  Structural mass fraction ~30% of GTOW
Rocket
Airbreather
Rocket vs. Airbreather: Weight and Volume

## Slide 35
  Driven by descent
  Low ascent heat load due to short ascent time and trajectory
  Driven by ascent, descent, and cruise
  High heat load due to long ascent and cruise time
Airbreather
Rocket
Rocket vs. Airbreather: TPS

## Slide 36
  Blunt, due to desire for high descent drag and low heat flux
  Sharp, due to low drag, low thickness-to-chord ratio
  High heat flux
Airbreather
Rocket
Rocket vs. Airbreather: Leading Edges
r = 0.030 in.
r = 6 in. - 10 in.

## Slide 37
  Propulsion and airframe not highly integrated
  Propulsion and airframe highly integrated
  Hot wings and control surfaces due to thin cross sections and high heat flux and heat load
Airbreather
Rocket
Rocket vs. Airbreather: Structures

## Slide 38
Large thermal gradients
  Tank / outer surface
  Control surfaces / actuators
Thin cross sections at high mechanical loads
High mechanical loads at elevated temperatures
Stability of the outer mold line (OML) shape
  Performance
  Non-ablative leading edge
  Steps and gaps (sneak flow and heating)
Thermal expansion of the propulsion system
Long times, elevated temperatures, oxidizing environment
Thermal-Structural Challenges

## Slide 39: Why CMC Hot Structures?
Hot structures provide ~ 25% weight savings over insulated cold structure
High-performance vehicles utilize high specific strength/stiffness materials
  Aluminum (Al)
  Composites: carbon fiber reinforce polymers (CFRP)
  Titanium (Ti)
  Beyond Ti use temperatures (~Mach 5), often utilize superalloys, refractory metals, and active cooling – not high specific strength/stiffness
  Refractory-composite (C/C, C/SiC, SiC/SiC, etc.) hot structures extend high specific strength/stiffness structures to 3000°F (1650°C) and above
Reduced deflections
MMC
Multi-Use
Single-Use /Ablator
C/C
Ceramics
Superalloys
Specific
strength
(strength
/density)
SiC/SiC
Ti
C/SiC
Goal: High specific strength & high temperature
Temperature, °F
CFRP
Al
UHT Ceramics
Steel plate after 2200°F (1200°C) exposure
> 0.5 in. (1.25 cm) residual deformation
MMC: Metal matrix composite
C/SiC: Carbon/silicon carbide
UHT: Ultra high temperature
Note: 2200°F is above the normal use temperature of steel

## Slide 40
Introduction
TPS and Hot Structures Components
  Leading edges
  Acreage TPS / aeroshell
  Control surfaces
Key Technical Challenges
Concluding Remarks
Outline

## Slide 41
Nose ~ 5000 Btu/ft2-sec
Wing ~ 500 Btu/ft2-sec
Cowl ~ 50,000 Btu/ft2-sec
Typical Ascent Leading-Edge Heat Flux for SSTO
In comparison, Shuttle Orbiter leading edge ~ 70 Btu/ft2-sec, CEV ~ 700 Btu/ft2-sec
500 Btu/ft2-sec ~ 567 W/cm2

## Slide 42
Heat flux
Temp.
Active cooling
Semi-passive (heat pipe)
Passive
Single use
Multi- use
Increased cost, complexity, weight
Ablator
Leading-Edge Thermal Management Options
There are multiple options to manage the intense heating on sharp leading edges

## Slide 43
Heat flux, Btu/ft2-sec
Radius, in.
Heat flux ∝
1
radius
1-in. radius, 500 Btu/ft2-sec
Leading-Edge Radius Effect on Heat Flux
10 in. = 25.4 cm
500 Btu/ft2-sec ~ 567 W/cm2
Notional flight conditions

## Slide 44
Sharp LE, hypersonic
vehicle
Upper
Surface
Lower
Surface
Shuttle
Orbiter
Heat
Flux
Chordwise position
Leading edge
Chordwise position
Leading-Edge Heating
Sharp leading edges produce intense, localized heating

## Slide 45
Property: Emissivity ()
qconv,surf = qrad,out =  Treq
qrad, Btu/ft2-sec
4000
3000
2000
1000
0
20
40
60
80
100
Radiation Equilibrium Temperature (Treq), °F
 = 0.1
 = 0.3
 = 0.5
 = 0.8
 = 1.0
4
High emissivity coatings
High emissivity coatings are very important to keep temperatures survivable
3000°F ~ 1650°C
100 Btu/ft2-sec ~ 113 W/cm2
100 W/cm2 ~ 88 Btu/ft2-sec

## Slide 46
Heat pipes reduce leading-edge temperatures to reuse limits of materials
Heat-Pipe-Cooled (Semi-Passive) Leading Edge
National Aerospace Plane (NASP)
Heat-pipe-cooled leading edge

## Slide 47
Vapor flow
Liquid flow
Container
Wick
Working fluid
Heat input
Heat output
Evaporator
Condenser
Heat-Pipe Operation
Heat pipes transfer heat isothermally by the evaporation and condensation of a working fluid

## Slide 48
Ts = Surface temperature
Treq = Radiation equilibrium temperature
Leading-Edge Heat-Pipe Operation

## Slide 49
Hastelloy-X container
Sodium (Na) working fluid
Leading edge
Heat pipe
Leading-Edge-Shaped Heat Pipe
Heated region
Heat pipe results in an isothermal leading edge

## Slide 50
Introduction
TPS and Hot Structures Components
  Leading edges
  Acreage TPS / aeroshell
  Control surfaces
Key Technical Challenges
Concluding Remarks
Outline

## Slide 51: Recombination (Catalytic) Efficiency
Dissociated species in hypersonic flow
Recombination
  Includes flow and surface
  Can be exothermic
  Si(g) + O SiO, ∆H = -605 Btu/mol (-638 kJ/mol)
(kft/sec ~ Mach)
Aerothermal heat flux calculations should assume partially-catalytic surface – higher heat flux is NOT always more conservative
Arc-jet test
Mach 4
 = 0.84
40
30
10
20
0
0.001
1
0.01
0.1
Btu/ft2-sec
Recombination efficiency
Non-catalytic
q = 10.1 Btu/ft2-sec
Catalytic
q = 28.3 Btu/ft2-sec
NASA 1958 Technical Memorandum
https://ntrs.nasa.gov/api/citations/19930085278/downloads/19930085278.pdf)

## Slide 52
Catalytic vs. Non-Catalytic Heat Flux
~1200°F (650K)
difference
2000K
~ 3150°F
1350K
~ 1970°F
SiC-coated surface is essentially non-catalytic
Copyright and courtesy of ArianeGroup
(kft/sec ~ Mach)
Uncoated C/C, g ~ 1 (g is catalycity)
Coated C/C, g = very low
Non-catalytic wall (glass)
Oxides
Catalysts (metals)
Krasnov, N. F. Aerodynamics. Translated by T. S. Patel. Edited by V. S. Kothekar. New Delhi: Amerind Publishing Co., 1978. Originally published 1971. Translated by NASA, open source.
https://archive.org/details/n.-f.-krasnov-aerodynamics-ntt-amerind-1978/page/665/mode/2up
Normalized heat flux
Thierry Pichon, "IXV CMC Thermal Protection System: Post Flight Preliminary Analysis”, International Astronautical Congress, Guadalajara, Mexico, Sept. 25-30, 2016
Fully catalytic assumptions can excessively over-predict surface temperatures

## Slide 53
Space Transportation System (STS) - 114
Insulator attached directly to cold structure to form outer mold line (OML)
Transfer aerodynamic loads to structure
Strain isolation required
Segmented (~ 6 in. x 6 in. or ~ 15 cm x 15 cm)
Insulated Structure
Tile with high emissivity coating
Damaged tile post-flight

## Slide 54
CMC Standoff TPS on Intermediate eXperimental Vehicle (IXV)
Used by permission of ArianeGroup

## Slide 55
Aeroshell carries aero and vehicle axial loads
Insulation incorporated or separate
Potential for reduced weight
Carbon/Carbon Aeroshell
DARPA/AF Falcon HTV-2
Load-Bearing Aeroshell

## Slide 56
Introduction
TPS and Hot Structures Components
  Leading edges
  Acreage TPS / aeroshell
  Control surfaces
Key Technical Challenges
Concluding Remarks
Outline

## Slide 57: Need for a Damage-Tolerance Approach (DTA)
Strength-based approach (SBA)
  Good for initial structural sizing
  Can provide inaccurate failure predictions from stress concentrations (cannot accurately predict)
  Cannot accurately predict crack advance: Manufactured parts containing cracks generally rejected
  Needs to be supplemented with a
  damage-tolerance approach
Damage-tolerance approach (DTA) (realistic goals)
  Apply at stress concentrations and manufacturing defects
  Accurately predict onset (stress concentrations) and growth (identified defects) of damage
  Utilize a no-growth philosophy for C/C and CMCs
  Inform part accept/repair/reject decisions
DTA can increase production yield, structural integrity, and vehicle life

## Slide 58
Disadvantages
  Heavy
  Little thermal margin
  Thick cross section
Tile
Metal or polymer matrix composite (PMC)
Tiles on orbiter elevons
Insulated Control Surface
U. Trabandt, T. Schmid, and E. Werth, “CMC and Metallic Hot Structure Hybrid Components for RLV,” 54th International Astronautical Congress, Breman, Germany, 2003.
Advantages
  Suitable for very large structures
  Minimal thermal expansion issues

## Slide 59
Advantages
  May not require TPS on upper surface
  More affordable manufacturing for large structures
  Replace CMC leading and trailing edges if damaged
Disadvantages
  Thermal growth mismatch between metal/PMC and CMC
  Weight increase 30% - 40% over all CMC
  Insulation of box structure leads to reduced thickness and small moment of inertia or a thicker cross section
CMC
Metal
or PMC
Hybrid (Material System) Control Surface
C/C
Haynes 230
X-43

## Slide 60
Advantages
  Lowest weight and thin cross section
  Minimal thermal expansion mismatch problems
  Thermal margin
  CMC has sufficient strength, stiffness, and damage tolerance for torsional and bending loads
  No external insulation
Disadvantages
  High manufacturing/tooling costs for box structure
  Challenging for very large structures
  Limited repair capability
  Manufacturing risk in case of production damage
  Access for coating, inspection, and maintenance of internal areas
  Tolerance stack-up of fasteners
CMC
CMC Hot-Structure Control Surface
U. Trabandt, T. Schmid, and E. Werth, “CMC and Metallic Hot Structure Hybrid Components for RLV,”
54th International Astronautical Congress, Breman, Germany, 2003.
Key Point: Do not design (and build and fly) a structure that we cannot model

## Slide 61
Introduction
TPS and Hot Structures Components
Key Technical Challenges
Concluding Remarks
Outline

## Slide 62
CMCs are the family of materials that will enable hypersonic vehicles
For most hypersonic vehicles, there are two key materials and structures technical challenges
Leading edges
Acreage
Hot structures
Propulsion system
Hypersonic Vehicles

## Slide 63
  Oxidation resistance (CMCs containing SiC)
    SiC works very well up to ~ 3000°F (1650°C), depending on temperature and pressure
    Is reusable, but number of cycles limited and must be verified
Passive oxidation (low temperature or high pressure)
    SiC(s) + 2 O2(g) SiO2(s) + CO2(g)
Active oxidation (high temperature or low pressure)
    SiC(s) + 1.5 O2(g) SiO(g) + CO2(g)
  Above ~ 3000°F (1650°C), but also function of pressure, no reusable solutions exist
  Challenges
Testing in relevant environments
Cycles under combined load
Multi-mechanism-driven failure
Accurate life prediction
Physics-based material limitations
Key Technical Challenge: Environmental Durability
Multiple cycles and increased duration increase environmental durability challenges
Failed test article due to active oxidation

## Slide 64
Chart: 
Starfire SMP-10 (PCP) based CMC with boride and carbide fillers tested in NASA Langley HyMETS arc-jet
250
500
750
1000
1250
1500
1750
Time, sec
Arc-jet testing of MT Aerospace C/SiC in the German PWK2 facility
Arc-jet testing of UHTC for the SHARP-B1 flight test at NASA Ames
~700°F / 4 sec.
Temperature, °F
Current (Amps), Voltage (Volts)
Voltage
Current
Temperature
Comparison of active and passive oxidation of sintered SiC
Active
Passive
Glass, Ref. 6
Infed, Ref. 1
Kolodziej, Ref. 7
Temperature Jump Observed in Multiple Arc Jets
Si

## Slide 65: Key Technical Challenge: Hot-Structure Manufacturing
A state-of-the-art material is not the same thing as a state-of-the-art structure – big difference
If we can manufacture it (well) and analyze it (accurately), it will perform as expected
In almost every program in which I've been involved,
it is manufacturing that comes up and bites us
The manufacturing challenges (MRL) are often under-estimated due to a focus on demonstrating performance (TRL)
Adopting the suggested AMSH Gates for Transitioning CMCs (next chart) will significantly improve cost and schedule for transition to flight
Credit: David Glass
MRL = manufacturing readiness level
TRL = technology readiness level
AMSH = Applied Materials for Space and Hypersonics

## Slide 66: AMSH Gates for Transitioning CMCs
Gate1 (G1): Locked-down manufacturing process – requires iterative process with manufacturing and testing
G2: Material property database utilizing a locked-down manufacturing process
  After database is generated, equivalency testing can be used to gradually transition improved processes
G3: Complex-shaped structure, at appropriate scale, manufactured utilizing the locked-down manufacturing process
  Example manufacturing demonstration: C-channel, saddle, and I-beam
G4: Thermal-structural tests and corresponding analyses of complex structures validating manufacturing and material properties
Demonstrated manufacturing capability (validated via test and analyses) at desired scale and complexity should be a required gate before consideration in a flight program
Saddle
C-channel
I-beam
Can extract sub-elements from these
Chemical vapor infiltration (CVI) C/SiC I-Beam
30 in. x 16 in. x 10 in.
May do some gates in parallel or different order
30 cm x 30 cm x 5 cm
12 in. x 12 in. x 2 in.
24 in. x 16 in. x 8 in.
76 cm x 41 cm x 25 cm
61 cm x 41 cm x 20 cm

## Slide 67
Densification of thick parts: properties function of thickness
Complex curvature and closure
Large scale (equipment, power, uniformity, etc.)
Delamination, poor bonds, voids, and defects
Tooling
Machining
Assembly methods, joints, and attachments
Tolerances
Reproducibility / consistency
Fabrication modeling
Design of manufacturable structures
Nondestructive inspection
Repair
Affordable (cost and schedule) manufacturing techniques (often-overlooked and typically addressed late in the development cycle)
Manufacturing Challenges
Years of manufacturing experience and building-block testing are required before complex structures can be successfully manufactured at scale and flown
C/C closure
Credit: C-CAT
X-38 C/SiC body flaps
Credit: “CMC-X38-Bodyflaps” by MT Aerospace AG, Augsburg, Germany licensed under CCA 3.0.
Manufacturing challenges are process-dependent

## Slide 68: Successfully Transitioning Hot Structures to Flight Vehicles
Components
Subcomponents
Coupons
Elements
G1: Locked-down process
G2: Material databases
G3: Fabrication of complex parts at scale
G4: Thermal-structural tests with model correlation
Science & technology (S&T) “fill” the toolbox (independent of flight/vehicle requirements)
Transitioning hot structures to flight: Vehicle & flight requirements inform TRL/MRL advancements to fill gaps
Caution: Jumping straight from a material to flight test can lead to over-estimation of MRL & TRL
No flight requirements
Credit: “CMC-X38-Bodyflaps” by MT Aerospace AG, Augsburg, Germany licensed under CCA 3.0.
Toolbox
May execute some gates in parallel or different order
Flight requirements
Flight hardware
Iterative process

## Slide 69: Manufacturing is the Biggest Challenge, Not Performance
If we can manufacture it (well) and model it (accurately), it will perform as expected
HTV-3X
IXV body flap post-flight
IXV post-flight
Atmospheric flight
Credit: DARPA
Credit: David Glass
Atmospheric reentry
Intermediate eXperimental Vehicle (IXV)
Credit: David Glass
Body flaps for different applications are very relevant because manufacturing is the biggest challenge

## Slide 70
  Thermal loads
  Thermal gradients
  Mechanical loads
  Acoustic and vibration loads
  Pressure (oxidation)
  Combined loads
  Number of cycles
Operation has a significant impact on our ability to use these materials as structures on flight vehicles
Will Hot Structures Meet Flight Requirements?
Testing at NASA Armstrong Flight Research Center (AFRC)

## Slide 71
How do we qualify the vehicle for flight?
We are unable to test many components in relevant, combined loads, environments (even small scale)
  Thermal, mechanical, plasma, shear, oxygen partial pressure, vibration and acoustic, etc.
  Apply appropriate boundary conditions over entire structure
  Thermal gradients (spatial and temporal) from boundary layer transition
Extensive testing is required
Performance testing and benchmarking for analyses
Building block approach
Testing
We cannot simulate this in ground tests
Arc-jet test of sharp leading edge
Material / coupon test
Component
test
Sub-element test
Test as much as you can, and still include adequate margins for uncertainties
Testing at NASA AFRC

## Slide 72
Introduction
TPS and Hot Structures Components
Key Technical Challenges
Concluding Remarks
Outline

## Slide 73
Hypersonic vehicles will require us to move beyond an insulated aluminum “airplane” to a vehicle with multiple TPS and hot-structure approaches
Our ability to build and fly these vehicles successfully will depend on our ability to utilize multiple types of CMC structures, first having solved the environmental durability and manufacturing challenges
Concluding Remarks
Additional details can be found in AIAA-2008-2682