## Slide 1
xEVA Systems All Hands –
EVA Fire Lessons Learned
09/15/26
Presented by:
Jonathan Tylka
NASA White Sands Test Facility
Materials and Components Laboratories
Trade names are used in this presentation for identification only. Their usage does not constitute an official endorsement, either expressed or implied, by the National Aeronautics and Space Administration.

## Slide 2: How Do We Typically Prevent Fires?
Air (21% oxygen)
Forest
Carpet
Furniture
Cigarette butt
Spark from fireplace
Matches
Fuel
Heat
Oxidizer
It’s Harder With An Oxygen System
100% oxygen
System components
Softgoods
Metal bodies
Lubricants
Contaminants
Ignition sources
Particle impact
Heat from rapid pressurization of O2
Electrical arc/spark

## Slide 3
“Only We Can Prevent Spacecraft Fires”

## Slide 4: Aerospace Fire History
Apollo 1
1/27/1967
Apollo 13
4/14/1970
The EMU Fire
4/18/1980
1950 |  | 1960 |  | 1970 |  | 1980 |  | 1990 |  | 2000 |  | 2010 |  | 2020
SpaceX F9-29
9/1/2016
Altitude Chamber Fire
3/23/1961
X-1, #3
11/9/1951
MIR Fire
2/24/1997
Cygnus Orb-3
10/28/2014
C204
4/20/2019

## Slide 5
How Did We Get Here…

## Slide 6: An EMU Fire Analogy: Mobile Oxygen Storage Tank Fires
Notes: During August of 2007 a Mobile Oxygen Storage Tank was being tested at Shepherd AFB. The tanks were filled with approximately 2,400 psi of 94.7% oxygen when an operator opened a ¼-turn ball valve that allowed the gas to flow into the stainless steel manifold, valves, and gages. A fire occurred which destroyed the unit. No one was injured in the fire.
Subsequent investigation revealed that the manifold system and particularly the gages were contaminated with hydrocarbon oil and that the heat from rapid pressurization ignited the oil which propagated and damaged the system.
The gages were calibrated with oil and subsequent attempts to clean them were unsuccessful.

## Slide 7: Mobile Oxygen Storage Tank Fires
Notes: During August of 2007 a Mobile Oxygen Storage Tank was being tested at Shepherd AFB. The tanks were filled with approximately 2,400 psi of 94.7% oxygen when an operator opened a ¼-turn ball valve that allowed the gas to flow into the stainless steel manifold, valves, and gages. A fire occurred which destroyed the unit. No one was injured in the fire.
Subsequent investigation revealed that the manifold system and particularly the gages were contaminated with hydrocarbon oil and that the heat from rapid pressurization ignited the oil which propagated and damaged the system.
The gages were calibrated with oil and subsequent attempts to clean them were unsuccessful.

## Slide 8
Notes: During August of 2007 a Mobile Oxygen Storage Tank was being tested at Shepherd AFB. The tanks were filled with approximately 2,400 psi of 94.7% oxygen when an operator opened a ¼-turn ball valve that allowed the gas to flow into the stainless steel manifold, valves, and gages. A fire occurred which destroyed the unit. No one was injured in the fire.
Subsequent investigation revealed that the manifold system and particularly the gages were contaminated with hydrocarbon oil and that the heat from rapid pressurization ignited the oil which propagated and damaged the system.
The gages were calibrated with oil and subsequent attempts to clean them were unsuccessful.

## Slide 9
Improper reaction – could have resulted in injury or death
Suffered severe injuries - hospitalized
Proper reaction – individuals exited the room to safety
6
9
7
8
1
4
5
2
3

## Slide 17: Characteristics of Nonmetals vs. Metals
Nonmetals | Characteristic | Metals
Low | Thermal Conductivity | High
Low | Ignition Temperature | High
Low | Combustion Temperature | High
Slow | Combustion Speed | Fast
Gaseous | Combustion Products | Liquid
Minor | System Components | Major

## Slide 18: SOP Regulator Module Post-Fire

## Slide 19: SOP Regulator Module Metals

## Slide 20: SOP Regulator Module Softgoods
Buna-N Burning
1000 psi - 100% Oxygen
PTFE Burning
1000 psi - 100% Oxygen

## Slide 21: Suspected Causes of the Fire
Heating by compression or shock of a thin section of aluminum between the flow restrictor passage and the adjacent cavity.
Heating by compression or shock of contaminants in the flow restrictor.
Heating of internal surfaces through mechanical shock of incoming high‑pressure oxygen, or heating of particles.
Similar heating of shut‑off valve o‑rings.
A conclusive cause was not established

## Slide 22: Short and Long Term WSTF Impact
At WSTF Over 2000 tests were performed on the batch lot of remaining regulators by June 1980
No catastrophic reactions were noted on any other SN from the failed batch lot of regulators
Over 7000 diagnostic tests were performed on redesigned regulators by April 1981
In 1981, NASA Headquarters funded WSTF testing to develop a greater understanding of potential ignition mechanisms in oxygen systems
Test program led by Frank Benz (NASA, WSTF) focused on three types of ignition
  Promoted combustion for determining absolute flammability of metallic materials
  Friction heating ignition from friction between rotating metallic components
  Particle impact ignition by metallic particulate in high-velocity oxygen
Led to our current understanding of oxygen system ignition mechanisms effecting metals
Test systems had major impacts on space shuttle flow control valve, space shuttle high pressure oxygen turbopump bearing testing, and Space Shuttle EMU
These systems are still operated and improved by WSTF to this day. Flight rationale on all major flight projects using oxygen at NASA relay on historical or application specific test data.
Having these systems ready is important for development of new systems and recovery from anomalies

## Slide 23: Board Recommendations/ Long Term Impacts

## Slide 24: Board Recommendations
11 total recommendations from the investigation board
4 Primary categories of recommendations:
  Design Improvements to minimize ignition risk
    Reduce entrapment points and thin cross sections
  Materials changes to maximize oxygen compatibility
    Body material changed from Aluminum to Monel
  Increase manufacturing and inspection quality
    Perform x-ray inspection. Consider neutron radiography to evaluate softgood condition
  Clarify NASA standards and create design guidelines

## Slide 25: Standards Development
Elements of todays primary oxygen standards are a direct result of the EMU fire.
Standards influenced include:
  NASA/TM-2007-213740- Guide for Oxygen Compatibility Assessments on Oxygen Components and Systems
  NASA-STD-6016C- Standard Materials and Processes Requirements for Spacecraft
  NASA-STD-6001B- Flammability, Offgassing, and Compatibility Requirements and Test Procedures

## Slide 26: Design Guidelines

## Slide 27: Future

## Slide 28
Be Prepared for fires during operations and tests when using hardware with oxygen
  Use good Facility Design, System Design, PPE, Hazard Controls, Procedures, Cleanliness- personal/system
Materials choices directly affect system mechanical performance and fire risk
Safe use of flammable materials in oxygen service is possible if ignition mechanisms are understood and controlled
Training is essential to understanding safe design, operations, and maintenance of oxygen systems. Not just for engineers, but technicians and operators also…
  The most common time for fire in O2 systems is commissioning and after maintenance
  Materials substitution of softgoods and lubrication are most likely to happen during maintenance
Documentation of the reasons for design decisions are very important to future teams
Schedule pressure is not a valid reason to skip steps that are safety critical
Key Points To Remember

## Slide 29: Key Points To Remember
Oxygen Compatibility Assessments (OCAs) are the tool for identifying and mitigating hazards in oxygen components and systems as designed.
OCAs are not a replacement for rigorous qualification and acceptance testing for systems as-built using oxygen!!!
  Testing and operating with oxygen in systems prior to flight is essential to understand the unique interactions between components and materials configuration.
  Think about the effect of off-nominal conditions and contamination upfront
In the lead up to an anomaly there are usually many overlapping factors. Normalizing of deviation, and missed mechanical performance symptoms are almost always present prior to failure.
  Tear down of hardware is essential to identify mechanical wear and partial ignitions
Historical failures have come at great cost, and taught us what to avoid in the future
  Failures in flight are seldom cost effective
Never have the crew screen for your failures

## Slide 30
Final Take Away…
Future Success Continuously Depends on Your Present Decisions
The most potent indicator of future catastrophe is arrogance born of present success.
– Joe McMann

## Slide 31: Acknowledgements
The following people were instrumental in researching this presentation and providing historical perspective:
Colin Campbell
Joel Stoltzfus
Mike Pedley
Woody Berenger
Steve Peralta
Joe Nowetner
Joe McMann
Mike Mannon
Thank you to:
Alex Kanelakos and Tim Hall for organizing this talk
John Moore for SOP curation @ JSC